SECTION 712

MISCELLANEOUS

Special Provision

712-2.13 GABIONS.  Add the following:

PVC Coating:  Coat 0.02 inches thick. Use fusion bonded PVC material.  Coating may be black, gray or green.

a.	Specific Gravity: Between 1.3 to 1.4, ASTM D 792

b.	Abrasion Resistance: The percentage of weight loss less than 12%, when tested according to ASTM D 1242, Method B at 200 cycles, CSI-A Abrader Tape, 80 grit.

c.	Brittleness Temperature. Not higher than 15F, ASTM D 746.

d.	Tensile Strength.  Extruded Coating (not less than 2.980 psi. ASTM D 412).  FUSION Bonded Coating (not less than 2275 psi. at 100 percent strain, ASTM D 638).

e.	Modulus of Elasticity. Extruded Coating (not less than 2,700 psi. at 100 percent strain, ASTM d 412).  Fusion Bonded Coating (not less than 1980 psi. at 100 percent strain, ASTM D 638).

f.	Ultraviolet Light Exposure.  A test period of not less than 3,000 hours, using apparatus type E at 63 C, ASTM G 23.

g.	Salt Spray Test.  A test period of not less than 3,000 hours, ASTM B 117.

After exposure to ultraviolet light and salt spray test as specified above, the PVC coating shall not show cracks, blisters, splits, or noticeable change of coloring (surface chalk).  In addition, the specific gravity shall not change more than 6%, resistance to abrasion shall not change more than 10%, and tensile strength shall not change more than 25% from initial values.