- SECTION 712

MISCELLANEOUS

Special Provisions

Add the following subsections:

712-2.19 LOW-VISCOSITY RESIN. Meet AASHTO M 235, Type IV, Grade 1, with the following revisions:

Amend Table 1 as follows:

Replace "2.0[20]" with "0.105[1.05]" in the row labeled "Grade 1, max".

712-2.20 CONCRETE ANCHOR INSERTS.

- Coil Anchor Inserts. Use 1 inch diameter galvanized inserts with a minimum safe working load of 7,500 pounds.  Hot-dip galvanize anchors according to AASHTO M 111 or AASHTO M 232.

Threaded Anchor Inserts. Use 1 inch diameter galvanized ferrule inserts with a minimum safe working load of 6,500 pounds.

712-2.21 EPOXY FOR BONDING DOWELS. Use an epoxy cartridge system appropriate for the service temperature and ambient concrete temperature at the time of installation.

Use epoxy cartridge systems that meet the requirements of the “Acceptance Criteria for Adhesive Anchors in Concrete and Masonry Elements,” AC58, by the International Code Council Evaluation Service (ICC-ES) including the suitability requirements for creep, in-service temperature, dampness, freezing and thawing, and seismic tests.

1.	Certification. Furnish 5 copies of a Certified Test Report from the manufacturer or an independent testing laboratory containing a list of dimensional, chemical, metallurgical, electrical, physical, and other required test results of the specified material certifying that the product or assembly has passed all specified tests. Include the following:

a.	the project name and number;

b.	the manufacturer's name;

c.	the name of the product or assembly;

d.	a complete description of the material;

e.	country of origin;

f.	the lot, heat, or batch number that identifies the material;

g.	all required test results for the specified material from the same lot, heat, or batch defined in Subsection 712-2.21.1.f;

h.	a statement, signed by a person having legal authority to act for the manufacturer or the independent testing laboratory, that the test results show that the product or assembly to be incorporated into the project has been sampled and tested and the samples have passed all specified tests.

712-2.22  GRANITE All granite shall be of standard architectural grade, free of cracks, seams, or starts, which may impair its structural integrity or function. Color or other visual characteristics shall be indigenous to the particular material. Texture and finish shall be within the range of samples provided to and approved by the Engineer.

TABLE 712-4

PHYSICAL REQUIREMENTS

| PROPERTY | RESULT | ASTM TEST METHOD |
| --- | --- | --- |
| Absorption by weight, max, % | 0, 40 | C97 |
| Density, min., lb/ft3 | 160 | C97 |
| Compress., Strength, min. psi | 19000 | C170 |
| Modulus of rupture, min, psi | 1500 | C99 |
| Abrasion resistance, min, haA | 25 | C241 |
| Flexural Strength, min, psi | 1200 | C880 |