SECTION 730

SIGN MATERIALS

Special Provision

Delete Subsection 730-2.05 and replace with the following:

730-2.05 DELINEATOR, FLEXIBLE.

- Delineator, Flexible shall be a two part system consisting of a drivable ground anchor socket and a replaceable, impact-resistant flexible post. Delineator, Flexible shall be Carsonite Composites Flexguard CFGR0, or approved equal. The system shall have the following properties:

- Post. The post shall be a flexible polymer material meeting the dimensions and colors shown on the plans. The post shall be resistant to ultraviolet light, ozone, and hydrocarbon damage and remain flexible at a temperature of minus 40 °F. Provide posts with yellow reflective sheeting on both sides that are capable of self-erecting and remaining serviceable after 5 head-on impacts at 55 mph and 10 impacts at 35 mph with an automobile at an air temperature of plus 40 °F.

- Ground Anchor Socket. The ground anchor socket shall be comprised of rigid material that does not collapse or buckle when driven into dense soil. Metallic materials shall be galvanized for corrosion resistance.

53433-032013