SECTION 306

ASPHALT TREATED BASE COURSE

Special Provisions

306-2.01 MATERIALS.  Delete Aggregate and Asphalt  and replace with the following.

1. 	Aggregate.  	Conform to subsection 703-2.04.

2. 	Asphalt.  	The total asphalt cement content may be a combination of PG 52-28 and the asphalt binder in the existing asphalt or only PG 52-28. Documentation and conformance is only required for PG 52-28.  The Engineer may conditionally accept asphalt cement at the source.  Provide a manufacture’s certificate of compliance according to subsection 106-1.05, and test results of applicable quality requirements of Section 702 before shipping the material.

Add the following:

3. 	Anti-Strip.   As Required by the approved Job Mix Design

4. 	Recycled Asphalt Pavement (RAP).

Process existing pavement removed under subsection 202-3.05 so material passes the 1 ½” sieve.  Stockpile the material separately from the crushed aggregates for pavement.  Perform one gradation and one asphalt content test for every 1000 tons (megagrams) of RAP or a minimum of 10 sets of tests which ever is greater.

CONSTRUCTION REQUIREMENTS

306-3.01 COMPOSITION OF MIXES.  Replace this subsection with the following:  If recycled materials are used, submit process control data of the RAP and of the asphalt concrete aggregates supporting proposed job mix design gradations.

At least 15 calendar days before the production, submit the following to the Engineer:

1.	A letter stating the location, size, and type of mixing plant,

2.	The proposed gradation for the Job Mix Design, gradations for individual stockpiles with supporting process control information, and the blend ratio of each aggregate stockpile and RAP.  The proposed virgin aggregate gradation must meet the requirements of Table 703-3, Type II.

3.	Submit gradation and asphalt content process control data of RAP for the Job Mix Design.

4.	Provide representative samples of each of the aggregates in the blend.  Sample sizes:  100 lbs of each intermediate and/or coarse aggregate, 200 lbs of fine aggregate, 22 lbs of blend sand, and 200 lbs of RAP.

5.	A minimum of  3 gallons samples of asphalt cement proposed for use in the mixture, including the name of the product, the manufacturer, test results as required in Section 702, manufacturer’s certificate of compliance according to Section 106, and a temperature viscosity curve for the asphalt cement.

6.	A ½ pint sample of the anti-strip additive proposed, including the name of product, manufacturer, and manufacturer’s data sheet, and current Materials Safety Data Sheet (MSDS).

From this information, the Engineer will establish the Job Mix Design using ATM 417, which will become a part of the Contract.  The Job Mix Design shall meet the requirements of Type II, Class B in Table 401-1, Asphalt Concrete Mix Design Requirements, except Voids in Mineral Aggregate (VMA) and Dust / Asphalt ratio specifications do not apply.  RAP may be used in the mixture.  The design minimum  asphalt content (RAP residual plus PG 52-28) is 5 percent by weight of total mix and with 1/4 percent anti-strip by weight of PG 52-28.

Submit changes in the Job Mix design warranted by changes in the source of asphalt cement, the source of RAP, the source of aggregates, aggregate quality, aggregate gradations, or blend ratios, in the same manner as the original submittal.  A new Job Mix Design will only apply to asphalt concrete mixture produced after submitting the new aggregate gradation.

Approved Job Mix Designs will have the full tolerances shown in Table 401-2 applied and will not be limited to the broad band listed in Table 703-3.

306-3.02 WEATHER LIMITATIONS.  Delete the requirements of this subsection and substitute the following:  Apply the requirements of subsection 401-3.01.

306-3.03 STOCKPILING.  Delete this subsection in its entirety.

306-3.04 EQUIPMENT.  Add the following:  Apply the requirements of subsection 401-3.02 to equipment.

Add the following to item 1.:

If recycled materials are used, the asphalt plant shall combine RAP with asphalt concrete aggregates to produce a hot recycled asphalt treated base mixture.

Delete subsection 306-3.06 and substitute the requirements of subsection  401-3.09.

Delete subsections 306-3.08 and 306-3.09 and substitute the requirements of subsections 401-3.12 and 401-3.13.

Apply the requirements of subsections 401-3.07, 401-3.10, 401-3.11, and 401-3.16.

Add the following subsection:

306-3.12 PATCHING DEFECTIVE AREAS.  Remove ATB that becomes contaminated with foreign material, is segregated, or is determined to be defective.  Do not skin patch.  Remove defective materials for the full thickness of the course.    Coat edges with a tack coat conforming to Section 402 and allow to cure.  Place and compact fresh ATB to grade and smoothness requirements.

306-4.01 METHOD OF MEASUREMENT.

Change the third paragraph to read:

Anti-strip additive.  Will not be measured for payment, the cost of the anti-strip additive will be subsidiary to Item 306(2).

Add the following subsection:

306-4.02 ACCEPTANCE SAMPLING AND TESTING.  The Engineer will sample and test Asphalt Treated Base at 1000 ton intervals for acceptance.  The Engineer will make the results of the acceptance testing available to the Contractor within seven working days from the date of sampling.  Sample the blended virgin aggregate at the cold feed.  At the pre-paving meeting the Contractor may select the sample location of mix to determine the asphalt content.

Within 24 hours of final rolling, cut one 6 inch diameter core, full depth, from the finished mat to determine density.  Neatly cut the sample using a core drill at the randomly selected location marked by the Engineer.  Use a core extractor to prevent damage to the core.  Do not cut a sample over a bridge deck.

Apply Tolerances shown in Table 401-2 to test results to determine compliance with mix design.

The Engineer will test for density, gradation, and asphalt content as specified in subsection 401-4.02.

306-5.01 BASIS OF PAYMENT.  Add the following:  Anti-strip shall not be paid separately but shall be subsidiary to Item 306(1) ATB.

If the Mix Design requires more than 5.0% asphalt cement, only the quantity in excess of 5.0% shall be paid for at the Contract unit price as Item 401 (2) Asphalt Cement, PG 52-28.

Patching defective areas shall be subsidiary to Item 306(1).