Add the following Section:

SECTION 750

CAST STONE

Special Provisions

750-2.01   DESCRIPTION.	Cast stone is a highly refined architectural precast concrete frost resistant building stone manufactured to simulate natural cut stone.

750-2.02   GENERAL REQUIREMENTS.    Conform to the dimensions, forms and sizes as shown on the plans.  Meet the following:

1.	ACI 318 - Building Code Requirements for Reinforced Concrete.

2.	ASTM A 615/A 615M - Standard Specification for Deformed and Plain Billet-Steel Bars for Concrete Reinforcement.

3.	ASTM C 33 - Standard Specification for Concrete Aggregates.

4.	ASTM C 150 - Standard Specification for Portland Cement.

5.	ASTM C 270 - Standard Specification for Mortar for Unit Masonry.

6.	ASTM C 494 - Standard Specification for Chemical Admixtures for Concrete.

7.	ASTM C 642 - Standard Test Method for Specific Gravity, Absorption, and Voids in Hardened Concrete.

8.	ASTM C 979 - Standard Specification for Pigments for Integrally Colored Concrete.

9.	ASTM C 1194 - Standard Test Method for Compressive Strength of Architectural Cast Stone.

10.	ASTM C 1195 - Standard Test Method for Absorption of Architectural Cast Stone.

11.	ASTM C 1364 - Standard Specification for Architectural Cast Stone.

12.	ASTM D 2244 - Standard Test Method for Calculation of Color Differences From Instrumentally Measured Color Coordinates.

- Cast Stone Institute Technical Manual.

750-2.03   CAST STONE MATERIALS

1.	Portland Cement:  ASTM C 150, Type I, white or gray as required to match specified color.

2.	Coarse Aggregate:  ASTM C 33, except for gradation; granite, quartz, or limestone.

3.	Fine Aggregate:  ASTM C 33, except for gradation; natural or manufactured sands.

4.	Pigments:  ASTM C 979, inorganic iron oxides.

5.	Admixtures:

a.	ASTM C 494.

b.	Integral water repellants and other chemicals for which no ASTM standard exists.  Previously established as suitable for use in concrete by proven field performance or through laboratory testing.

- Water:  Potable.

- Reinforcing Bars:  ASTM A 615/A 615M, galvanized or epoxy coated.

750-2.04   MORTAR

1.	Mortar:  ASTM C 270, Type N.