SECTION 501

STRUCTURAL CONCRETE

Special Provisions

501-2.01 MATERIALS.  Add the following to the list of material specifications:

Flowable Fill Sand		Subsection 703-2.14

501-3.01 PROPORTIONING.  Add the following to Item 1 Contractor Mix Design:

Flowable Fill Mix Design.  The mix shall be proportioned to be non-segregating, free flowing, self consolidating, and low shrink slurry with a minimum unconfined compressive strength at 28-days of 100 psi as determined in accordance with ASTM D 4832.  The Contractor and supplier shall determine the materials and proportions used to meet the requirements of these specifications.  At least 21-days before placement of flowable fill, the Contractor shall submit a mix design to the Engineer and include the following information:

- Certification of compliance to the mix design requirements of this specification.

- Certification of compliance of the component materials used in the mix design relative to this specification and referenced specifications.

- Representative gradations for aggregate and proposed gradation limits for aggregates to be used in the flowable fill.

- Performance characteristics of the hardened flowable fill to include compressive strength of specimens.  Tests for compressive strength shall be reported for ages of 1-day, 7-days, and 28-days.

- Unit weight of all compressive strength specimens at time of testing and corresponding average unit weight.

No flowable fill shall be placed until the mix design has been reviewed and accepted by the Engineer.

501-3.07 FORMS.  Add the following:

Forming for the Flowable Fill shall be approved by the Engineer.

501-3.10 CURING CONCRETE. Add the following:

Flowable Fill shall cure undisturbed for at least 24 hours.

501-5.01 BASIS OF PAYMENT.

Add the following pay item:

Pay Item No.	Pay Item	Pay Unit

501(22)	Flowable Fill	Cubic Yard