SECTION 729

GEOSYNTHETICS

Special Provisions

Add the following subsection:

729-2.06 IMPERMEABLE MEMBRANE.  The membrane shall be 20 mil Herculiner manufactured from High Density Polyethylene by In-Line Plastics, Inc. or approved equal.

The liner shall meet the following requirements:

| Requirement | Extruded Fabric |
| --- | --- |
| Cold crack (ASTM D2136) | -60F |
| Black carbon content (ASTM D1603) | 2% or greater |
| Carbon dispersion (ASTM D3015) | A-2 range |
| Tensile strength (ASTM D751A) |  |
| Mullen burst (ASTM D751A) |  |
| One inch tensile strength (ASTM D882) | 45 lbs. (Warp) |
| One inch elongation MD (Machine Direction) | 625% |
| Nominal thickness | 20 mil |
| Oil resistence (ASTM D471) | No signs of deterioration and more than 80% retention of tensile and seam strength after immersion for 30 days at 73F |