- SECTION 635

INSULATION BOARD

Special Provisions

635-2.01 MATERIALS.  Delete the “Insulation Board” item and replace with the following:

Insulation Board. The insulation boards shall be high density extruded polystyrene board stock, with a minimum full board size of 2’ X 8’. Compressive Strength to have a minimum value at ASTM D-1621, 60 PSI or 5 percent deformation. Water Adsorption to have a maximum percent by AASHOT M-230, 0.10 volume, and Thermal Resistance ( R), min R-Value at ASTM C-177, as specified 75 º F mean temperature, SF-Hr-ºF/BTU.

635-5.01 BASIS OF PAYMENT.  Add the following pay item:

Pay Item No.	Pay Item	Pay Unit

635(2)	Insulation Board, R=9	Square Foot