SECTION 635

INSULATION BOARD

635-2.01 MATERIALS.

Add the following to this subsection:

Insulation Board.  The insulation boards shall be high density extruded polystyrene board stock, with a minimum full board size of 2’x8’. Compressive Strength to have a minimum value at ASTM D-1621, 60 psi yield or 5 percent deformation. Water Absorption to have a maximum percent by AASHTO M-230, 0.10 volume,  and Thermal Resistance (R), min. R-Value at ASTM C-177, as specified 75°F mean temperature, SF-Hr-°F/BTU.

Special Provisions

635-4.01 METHOD OF MEASUREMENT.  Delete this subsection in its entirety and substitute the following:  By the cubic foot of insulation board, in place based on the nominal dimensions or the materials, or by the square foot of insulation board with the required “R” value in its final position, including transitions, regardless of thickness, complete and accepted.

Sand blanket material is subsidiary.

(8/23/00)R57USC

635-5.01 BASIS OF PAYMENT.  Add the following: Payment will be made under:

| - Pay Item | - Pay Unit |
| --- | --- |
| 635(2-20) Insulation Board, R=20 | Square Foot |
| 635(2-30) Insulation Board, R=30 | Square Foot |