SECTION 611

RIPRAP

Special Provision

611-1.01 DESCRIPTION.  Add the following:  This work shall also consist of placing Drain Rock and installing J-Hook Structures.

611-2.01 MATERIALS.  Add the following after the first sentence:  Apparent specific gravity will be determined by WAQTC FOP for AASHTO T85.

CR277-110705

Add the following to the list of material specifications:

J-Hook Rocks	         As shown in the Plans

Drain Rock	Subsection 703-2.13

611-3.01 CONSTRUCTION REQUIREMENTS.  Add the following:  J-Hook Structures shall be constructed according to the details shown in the Plans.  In stream channel fills, voids in the Riprap, J-Hook Structures and Drain Rock shall be filled with Selected Material, Type B.  Blend material prior to placing.  This material is intended to inhibit subsurface stream flow through the voids provided by typical riprap installations by adding a silty sandy gravel to fill the voids.

611-4.01 METHOD OF MEASUREMENT.  Add the following:

J-Hook Structure: By each J-Hook Structure complete in place.

Selected Material, Type B used to fill in the voids in stream channel fills will not be paid for directly, but will be subsidiary to 611 items.

611-5.01 BASIS OF PAYMENT.

Add the following pay items:

Pay Item No.	Pay Item	Pay Unit

611(9)	J-Hook Structure	Each

611(10)	Drain Rock	Cubic Yard