SECTION 727

SOIL STABILIZATION MATERIAL

Special Provisions

Add the following:

727-2.05 ROOT BARRIER.

- Root barrier materials shall meet the following requirements:

1.	Product standard of quality or approved equal:

a.	UB 18-2 root barriers by DeepRoot

b.	Shawtown EP Series root barriers by NDS, Inc.

2.	Material:  With ultraviolet (UV) inhibitors.

3.	Thickness:  Minimum 0.085-inch.

4.	Joining System:  Factory installed, interlocking joining mechanisms for easy assembly.

5.	Reinforcing Ribs:  Integral molded, vertical root deflecting ribs.

6.	Ground anchorage:  Ground locking anti-lift tabs or minimum 1/8 inch wide base flange.

7.	Panel Size:  Minimum 24- inch long by 18-inch deep.

55659-122512