SECTION 504

STEEL STRUCTURES

Special Provisions

504-2.01 MATERIALS.

Add the following:

Stainless Steel Fasteners:

Stainless steel bolts, nuts and washers shall provide AISI 316 stainless steel and shall conform to ASTM A193, B8M Class 1 and ASTM A194, 8M.

Delete Subsection 504-3.03 in its entirety and replace it with the following:

504-3.03 FINISH.

Perform work in accordance with safety regulations and guidelines of Federal, State and local agencies having jurisdiction.  Provide surface preparation and finishes in a controlled, suitable shop environment.

Provide finish surfaces of members exposed in final structure free of markings, burrs, and other defects.  Clean foreign matter, slag and weld splatter from steel members after fabrication is complete.  Complete welding before applying finish.

Surface Preparation:

- Blast clean steel after fabrication in accordance with SSPC-SP 10, Near-White Blast Cleaning.

- Galvanized steel surfaces to be painted shall be pre-cleaned with acid etched with 1 part commercial muriatic acid reduced by 2 parts water by volume (giving an approximate 10 percent solution of hydrochloric acid).  Preparation shall produce a “grit sandpaper” surface profile for anchoring top coats.

Shop-fabricated steel components shall be hot-dipped galvanized after fabrication in accordance with Section 716-2.07, to a minimum zinc coating thickness of 2.0 oz./sf.  The finish for manufactured connectors for wood construction shall be in accordance with Section 713-2.04.

Field Touch-Up Preparation:

- Clean new steel surfaces in accordance with SSPC-SP1.

- Wire brush cleaning (SSPC-SP2), power tool cleaning (SSPC-SP3), or commercial blast cleaning (SSPC-SP6) shall be required as necessary to remove all rust before field touch-up.

- Zinc shall have contact with bare metal to provide galvanic protection.

Field Finish Repairs:  Touch-up metal that has been hot dipped galvanized with zinc spray in accordance with ASTM A780.

57181-120111