Special Provisions

Replace Section 713 with the following:

SECTION 713

STRUCTURAL TIMBER

713-2.01 	GENERAL REQUIREMENTS. Furnish structural timber manufactured according to the Voluntary Product Standard PS 20 as published by the United States Department of Commerce.

Use timber free of heart center or pith of the log.

713-2.02 	SPECIES REQUIREMENTS. Furnish Douglas Fir-Larch as described in ASTM D 1165, unless otherwise noted.

713-2.03 	GRADE REQUIREMENTS. Furnish timber graded according to the West Coast Lumber Inspection Bureau (WCLIB) grading rules or the Western Wood Products Association (WWPA) grading rules. Meet the following minimum grade requirements, unless otherwise noted:

Dimension Lumber		No. 2 (WCLIB & WWPA)

713-2.04 	SURFACING AND SEASONING REQUIREMENTS. Furnish timber surfaced on four sides (S4S) when the wood moisture content is less than 19%, unless otherwise noted.

713-2.05 	INSPECTION, GRADE STAMPING, AND CERTIFICATION. Furnish timber inspected by the West Coast Lumber Inspection Bureau (WCLIB), Western Wood Products Association (WWPA), or the Pacific Lumber Inspection Bureau (PLIB). Ensure timber delivered to the project bears the certified lumber grade stamp provided by the inspecting agency. Provide grading certificates issued by either the inspecting agency whose stamp is shown on the timber, or by the lumber mill supervised by the inspecting agency including the following:

1.	Name of the mill performing the grading

2.	The grading rules being used

3.	The name and certification of the person doing the grading

4.	Signature of a responsible representative of the mill

5.	Date the timber was graded

6.	Grade, dimension, and quantity of timber

57109-080812