SECTION 670

TRAFFIC MARKINGS

Special Provisions

670-1.01 DESCRIPTION.  Delete this subsection in its entirety and substitute the following:  This work consists of furnishing, preparing and placing pavement markings at the locations shown on the Plans or as directed.  Meet these Specifications and the applicable portions of the Alaska Traffic Manual.

Durable pavement markings consist of either preformed marking tape or Methyl Methacrylate pavement markings at the Contractor’s option.  Once selected, only one durable pavement marking type shall be used throughout that section indicated on the Plans.

670-3.01 CONSTRUCTION REQUIREMENTS.  Delete Item No. 2 and substitute the following:

2.	Preformed Marking Tapes (PMT).  Apply the PMT material as directed by the manufacturer using the appropriate inlay method either (a) or (b) below.

Store PMT materials between 60  F and 85 F for at least 24 hours before installation.  During installation, maintain field stockpiles at the required storage temperature.

a.	Hot Inlay Method:  Use this method for applying PMT to new hot asphalt pavements where the temperature of the mat is above 140 F.  Embed the pavement markings in the asphalt concrete surface with a conventional steel wheeled roller.  Apply when the surface temperature of the mat is the warmest possible without deforming the marking.  The minimum allowable surface temperature, taken within 3/8 inch of the top of the mat is 140 F..

If the application of the PMT materials falls behind the paving operation to the extent that the markings are not being applied at the minimum acceptable temperature, slow the paving operation to match the rate of the marking laydown.  Resume full paving operations after demonstrating that skilled personnel are available to install the markings within the required temperature limits.

b.	Cold Inlay Method:  Use this method for applying PMT to existing pavements where the temperature of the mat is below 140 F.  Ensure the surface is clean and dry and is at least 60 F and rising.  Groove in the markings below the surface of the asphalt.  The bottom of the groove shall have a smooth flat finish.  Accomplish this by using a gang stacked cutting heads having diamond tipped cutting blades.  Provide a space between each blade.  The rise between the finished groove and the blades shall be 10 mils.  Broom the surface clean.

Remove dust using compressed air.  Apply a coat of primer/adhesive activator according to the manufacture’s recommendations.  Install and roll the markings with a minimum 200 pound pneumatic roller.

Delete all paragraphs under item 4. Methyl Methacrylate Pavement Markings. and substitute the following:

a.	General.  15 days before starting work meet with the Engineer for a prestriping meeting.  At this meeting, do the following:

1.	Furnish a striping schedule showing areas and timing of work, placing materials and the Traffic Control Plans to be used.

2.	Discuss placement of materials, potential problems.

3.	Discuss work plan at off ramps, on ramps and intersections.

4.	Discuss material handling procedures.

5.	Provide copies of the manufacturer’s installation instructions and copies of the Material Safety Data Sheets.

b.	Manufacturer’s Representative.  Provide the services of a manufacturer’s representative (the “Manufacturer’s Representative”).  Ensure the Manufacturer’s Representative observes the application of the pavement marking materials.  Cooperate with the Manufacturer’s Representative and the Engineer to ensure that the materials are placed according to these Specifications and the manufacturer’s recommended procedures.

c.	Manufacturer Certified Installers.  Install methyl methacrylate pavement markings using only striping installers certified by the marking materials manufacturer for the specific striping material and method.  Submit these certifications to the Engineer at the Preconstruction Conference.

d.	Preparation.  Prepare the roadway surface to receive methyl methacrylate according to these Specifications and the manufacturer’s recommendations.  Clean and dry the roadway surface.  Completely remove contaminants such as dirt, loose asphalt, curing agents, surface oils, or existing road marking materials before applying pavement marking material.

e.	Application.  Apply methyl methacrylate marking material according to these Specifications and the manufacturer’s recommendations.  Use equipment designed and capable of properly mixing at the point and time of application and approved by the manufacturer for the type of product being installed.

For longitudinal markings use truck mounted automatic extrusion equipment capable of installing a double line in a single pass.  Use automatic bead applicators that place a uniform layer of beads on the lines.  Hand units will not be allowed.

For Transverse markings legends, symbols, and transverse markings use manual or automatic application equipment.  Stencils or extruders are required to form sharply defined markings

For inlaid applications use grooving equipment that produces a dry cut.  Use vacuum shrouded equipment or other equally effective containment procedures.  Install markings in the same work shift as the grooving operation.

(1)	Longitudinal Markings Surface Applied.  Apply markings for lane lines, edge lines, and centerlines to yield a minimum thickness of 90 mils as measured from the surface of the pavement.  Use Type B material, as specified in subsection 712-2.17.

(2)	Longitudinal Extruded Markings Inlaid.  Apply markings for lane lines, edge lines, and centerlines to yield a thickness of 250 mils as measured from the surface of the pavement.  Use Type b material.  Groove the area for the inlaid markings to a depth of 250 mils.

(3)	Transverse and Symbol Markings Inlaid.  Apply markings for onlys, arrows, stop bars, gore stripes, railroad symbols, and cross walks to yield a thickness of 250 mils as measured from the surface of the pavement.  Use Type C material, as specified in subsection 712-2.17.  Groove the area for inlaid marking to a depth of 250  mils.

(4)	Traverse and Symbol Markings Surface Applied.  Apply markings for onlys, arrows, stop bars, gore stripes, and cross walks to yield a thickness of 120 mils as measured from the surface of the pavement.  Use Type C material.

f.	Disposal of Waste.  Waste material becomes the Contractor’s property.  This includes grindings and removed marking material.  Do not dispose of or store stripe removal wastes material or asphalt grindings on State property.  Dispose of waste material according to applicable Federal, State, and local regulations.

g.	Sampling.  On the form provided by the Engineer, record the following readings, and the locations where they were taken, and submit them to the Engineer within 24 hours for evaluation.  Thickness of material and depth of slot are measured from the surface of the pavement.

(1)	For inlay applications, record the depth of the slot every 300 feet during the grinding operation.

(2)	For other longitudinal applications, measure the thickness of the lines (above the pavement surface), at the time of application, every 300 feet.

(3)	For surface applied transverse markings measure the thickness in three locations for each marking.

(4)	Inspect the markings initially, and again two weeks after placement, to ensure the material has cured properly.  Remove soft spots or abnormally darkened areas and replace with material meeting specifications.

(5)	Measure the retroreflecivity of each transverse marking at three locations, and of each line at intervals not to exceed 1,500 feet.  Take these measurements using a Delta LTL2000 Retrometer, a 100 foot retro-reflectometer, or approved similar device.  Perform testing within 72 hours of curing.

The Engineer may elect to use the Contractors readings or perform additional sampling.

670-3.04 PAVEMENT MARKING REMOVAL.  Add the following:  Coordinate removal work with construction activity.  Remove pavement markings the same day permanent markings are applied, unless otherwise directed.  Use vacuum shrouded equipment or other equally effective containment procedures.

Replace subsection 670-3.07 with the following:

670-3.07 TOLERANCES FOR LANE STRIPING.

1.	Length of Stripe.  ± 2 inches.

2.	Width of Stripe.  ± 1/8 inch.

3.	Lane Width. ± 4 inches from the width shown in the Plans.

4.	Stripes on Tangent.  Do not vary more than 1 inch laterally within a distance of 100 feet when using the edge of the stripe as a reference.

5.	Stripes on Curves.  Uniform in alignment with no apparent deviations from the true curvature.

6.	All Stripes.  Keep the center of the stripe within 4 inches from the planed alignment.

7.	Double Stripes.  ± ¼ inches

8.	Thickness of surface applied.  Minimum specified to a maximum of + 30 mils.

9.	Depth of Inlay Slot.  Minimum 250 mils to a maximum of 290 mils.

10.	Thickness of Inlaid Marking Material.  Fill inlay area completely from the bottom of the inlay to the surface of the pavement.

If it is determined that the material is being placed too thin, or otherwise not to specification, make immediate adjustments to correct the problem.

Durable pavement markings applied by any method will be unacceptable if:

1.	The marking is not straight or wide enough.

2.	The thickness of the line is not uniform or less than specified.

3.	The top of the line is not smooth and uniform.

4.	The material is uncured.

5.	The material blackens or is inconsistent in color.

6.	The inlay slot is not ground to the specified depth.

7.	The inlay slot is not filled to the specified depth.

8.	The edge of the markings are not clear cut and free from overspray.

9.	The reflective elements are not properly embedded.

10.	The markings exhibit poor adhesion.

11.	The retro-reflectivity of the markings is less than specified and not uniform.

12.	The color is not as specified.

Perform repairs using equipment similar to the equipment initially used to place the materials.  Do not perform repairs in a “patch-work” manner.  If more than one repair is required in a single 300 foot section, grind and repair the entire section.

Add the following subsection:

670-3.07 PERIOD OF PERFORMANCE FOR PMT.  PMT pavement markings that become dislodged for any reason (including snow removal operations by the Department) within one year of installation shall be replaced at the Contractor’s expense.

PMT requiring replacement shall be grooved in using Method (b) above.

670-4.01 METHOD OF MEASUREMENT.  Add the following:

4.	Linear foot.  Durable Pavement markings will be measured by the 4 inch wide length of actual stripe applied.

Thickness will be measured from the top of the marking to the top of the pavement surface.  Marking material placed in a depression left by pavement line removal will not be included in measuring the thickness of the line.

670-5.01 BASIS OF PAYMENT.  Add the following:  There will be no separate or additional payment for the following:

	Over-runs of material caused by the variation of the gradation of the asphalt.

	Additional material required to achieve the thickness specified an open graded pavement.

Milling for installation of the inlaid markings is subsidiary to 670 items.  Payment includes costs associated with this item, including the removal of millings.

Traffic control for pavement markings will not be paid for directly but will be subsidiary to the pavement markings.  (01/04/06)R246usco04

Removal of conflicting marking will not be paid for directly, but will be subsidiary to the pavement markings.

Temporary markings will not be paid for directly, but will be subsidiary to the pavement markings.

Payment will be made under:

Pay Item No.	Pay Item	Pay Unit

670(13A)	Durable Pavement Markings Longitudinal	Linear Foot