SECTION 508

WATERPROOFING MEMBRANE

Special Provisions

508-1.01 DESCRIPTION.  Add the following:  remove the existing asphalt pavement surface and membrane waterproofing on the following bridge:

| - Bridge Number | - Bridge Name |
| --- | --- |
| 1025 | Resurrection Creek Bridge |

508-3.01 APPLICATION OF MEMBRANE WATERPROOFING.  Replace the last sentence of the first paragraph with the following:

Achieve the following results:

- Complete bond between the leveling course to the full concrete bridge deck.

- Complete bond between the membrane and the leveling course.

- Unbroken waterproof membrane in place between the leveling course and the asphalt overlay.

- Complete bond between the membrane and the asphalt overlay.

Replace the second paragraph with the following:

- Remove Existing Asphalt and Membrane Waterproofing.  Before applying membrane:

- Remove existing asphalt concrete down to the base concrete bridge deck.

- Do not employ removal methods that damage the concrete deck.

- Do not use a mechanical milling machine such as a reclaimer or planer.

- Prevent foreign material from entering stream.

Replace the fourth paragraph with the following:

- Sequencing of the Membrane.  When placing or overlaying membrane, observe the following:

- Apply tack coat to prepared concrete deck.

- Place 1 inch thick leveling course of Asphalt Concrete, Type II; Class B over deck tack coat.

- Place the membrane over 1 inch leveling course.

- Place Asphalt Concrete, Type II; Class B over membrane as shown.

Add the following:

- Overlaying and Protection of Membrane.  When placing or overlaying membrane, observe the following:

- Place membrane according to manufacturers recommendations and item 3 of this subsection.

- Allow membrane to cure enough to prevent damage.

- Place the asphalt surface course without membrane damage from paving equipment.

- Do not operate vehicles over placed membrane, except for the asphalt paver and trucks containing asphalt mix.

- Use only rubber-tired or rubber-tracked paving machines over the membrane.

- Use only steel wheeled rollers to compact the asphalt paving on the bridge decks.

- Do not use vibratory rollers with vibrator turned on.

508-5.01 BASIS OF PAYMENT.  Replace the second paragraph with the following:  Asphalt Concrete, Type II; Class B leveling course is paid for under the appropriate paving item.

Removal of existing pavement and waterproof membrane is subsidiary to Item 508(1) Waterproofing Membrane.