SECTION 712

MISCELLANEOUS

Add the following subsections:

712-2.19 Epoxy Resin.  Use a two component epoxy resin compound that will bond to an existing treated timber glu-lam deck and meet the following requirements:

Physical Properties (cured, 30 days, 1:1 mix ratio):

Tensile Strength							1460 psi				ASTM D638

Compressive Strength						5210 psi				ASTM D695

Flexural Strength							900 psi					ASTM D790

Durometer Hardness, Type D				42						ASTM D2240

Elongation									84%					ASTM D638

712-2.20 Epoxy Resin Adhesive.  Use a two component epoxy resin adhesive paste that will bond to an existing treated timber glu-lam deck and meet the following requirements:

Physical Properties (cured, 30 days, 1:1 mix ratio):

Tensile Strength							1790 psi				ASTM D638

Compressive Strength						2730 psi				ASTM D695

Flexural Strength							1622 psi				ASTM D790

Durometer Hardness, Type D				54						ASTM D2240

Elongation									3.2%					ASTM D638

57109-080812