## ITEM F-161	WIRE FENCE WITH STEEL POSTS (CLASS C AND D FENCE)

DESCRIPTION

161-1.1 This item covers the requirements for furnishing materials and constructing wire fences and gates with steel posts according to the details included herein and as shown on the Plans. The class of fence to be erected shall be either Class C, woven wire fencing surmounted by 2 strands of barbed wire, or Class D, 4 strands of barbed wire, as specified.

MATERIALS

161-2.1 WIRE.

- Woven Wire (Zinc-coated). Woven wire fabric shall meet AASHTO M 279, Design Number 726-6-12 ½, Grade 60, Coating Type Z, and Coating Class 3.

- Barbed Wire (Zinc-coated). Barbed wire shall meet AASHTO M 280, Design Number 12-4-5-14R, Standard Grade, Coating Type Z, and Coating Class 3.

- Barbed Wire (Aluminum-coated). Barbed wire shall meet AASHTO M 280, Design Number 12-4-5-14R, Standard Grade, Coating Type ZA, and Coating Class 60.

- Bracing Wire (Zinc-coated). Wire used for bracing shall be smooth galvanized wire, and shall meet AASHTO M 181, Tension Wire, except it may be 9-gage thickness.

161-2.2 FENCE POSTS, GATES, RAILS, BRACES, AND ACCESSORIES. These items shall be hot-dip galvanized steel, conforming to AASHTO M 181, Type 1, Grade 1 or Grade 2, and shall be the size shown on the Plans.

161-2.3 CONCRETE. Concrete shall be of a commercial grade with a minimum 28-day compressive strength of 2,500 pounds per square inch (psi) or an approved, pre-mixed, sacked concrete.

161-2.4 GATE LOCKS. Gate locks shall be provided for each gate and shall be brass, restricted-keyway padlocks with a shackle that is 3/8 inch in diameter having a closed clearance of 2-1/4 inches. The locks shall have control key removable cores and each lock shall have a separate replacement core. All cores shall be keyed differently. The Contractor shall provide 4 keys per lock and 2 core removal keys.

CONSTRUCTION METHODS

161-3.1 GENERAL. The fence shall be constructed according to the details on the Plans and as specified herein. The Contractor shall be responsible for establishing the fence alignment as shown on the Plans. After the fence line has been staked, and prior to fence installation, the Contractor shall review the alignment with the Engineer and make required adjustments to avoid conflicts.

When directed, the Contractor shall span the opening below the fence with barbed wire at all locations where it is not practical to conform the fence to the general contour of the ground surface because of natural or manmade features such as drainage ditches. The new fence shall be permanently tied to the terminals of existing fences whenever required by the Engineer. The finished fence shall be plumb, taut, true to line and ground contour, and complete in every detail. When directed, the Contractor shall stake down the woven wire fence at several points between posts.

When directed, in order to keep stock on adjoining property enclosed at all times, the Contractor shall arrange the work so that construction of the new fence will immediately follow the removal of existing fences. The length of unfenced section at any time shall not exceed 300 feet or such length that the stock can be kept in the proper field. The work shall progress in this manner and at the close of the working day the newly constructed fence shall be tied to the existing fence. Any openings in the fence shall be guarded when stock is using the adjoining property.

161-3.2 CLEARING FENCE LINE. The site of the fence shall be sufficiently cleared of obstructions, and surface irregularities. The fence line shall be graded so that the fence will conform to the general contour of the ground. The fence line shall be cleared to a minimum width of 10 feet on each side of the centerline of the fence. This clearing shall consist of the removal of all stumps, brush, rocks, trees, or other obstructions which will interfere with proper construction of the fence. Stumps within the cleared area of the fence shall be grubbed or excavated. The bottom of the fence shall be placed a uniform distance above ground, as specified in the Plans. When shown on the Plans or as directed by the Engineer, the existing fences which interfere with, the new fence location shall be removed by the Contractor as a part of the construction work unless such removal is listed as a separate item in the bid schedule. All holes remaining after post and stump removal shall be refilled with suitable soil, gravel, or other suitable material and compacted with tampers.

161-3.3 INSTALLING POSTS. All posts shall be spaced as shown on the Plans. Corner, brace, anchor, end, and gate posts shall be set in concrete bases as shown on the Plans. The top of the concrete shall be slightly above the ground surface, trowel finished, and sloped to drain. Post holes of full depth and size for the concrete shall be provided. All line posts may be either driven or set in dug holes to a penetration of 3 feet. All post setting shall be done carefully and to true alignment. Dirt removed for placing posts, anchor bars, flanges, etc., shall be replaced, tamped, and leveled. When posts are driven, care shall be exercised to prevent marring or buckling of the posts. Damaged posts shall be replaced at the Contractor’s expense.

161-3.4 BRACING. All corner, anchor, end, and gate posts shall be braced as shown on the Plans. Anchor posts shall be set at approximately 500-foot intervals and braced to the adjacent posts.

161-3.5 INSTALLING WIRE. All barbed wire and woven wire shall be placed on the side of the post away from the airport, or as directed by the Engineer, at the height indicated on the Plans. The woven wire shall be carefully stretched and hung without sag and with true alignment. Care shall be taken not to stretch the wire so tightly that it will break in cold weather or pull up corner and brace posts. All horizontal wires shall be fastened securely to each post by fasteners or clips designed for use with the posts furnished. The woven wire shall be wrapped around end, corner, and gate posts, and the ends of all horizontal wires shall be tied with snug, tight twists. The wire shall be secured to prevent slipping up and down the post. Barbed wire strands shall be stretched and each strand secured to each post to prevent slipping out of line or becoming loose. At end, corner, and gate posts the barbed wire shall be securely wrapped and anchored once about the post from outside and secured against slipping by tying the ends with snug, tight twists. However, on spans of less than 100 feet, both ends of the span need not be wrapped around the posts. The bottom wire of the woven wire fencing shall clear the ground by not more than 4 inches or less than 1 inch at any place.

161-3.6 SPLICING WIRE. Splices in barbed and woven wire will be permitted if made with an approved galvanized bolt-clamp splice or a wire splice made as follows: The ends of each wire shall be carried 3 inches past the splice tool and wrapped around the other wire for at least 6 turns in opposite directions. After the tool is removed, the space occupied by it shall be closed by pulling the ends together. The unused ends of the wire shall be cut off neatly.

161-3.7 INSTALLING GATES. The gates shall be hung on gate fittings as shown on the Plans. They shall be attached in such a manner that the gate cannot be lifted off the hinges. Gates shall be erected to swing in the direction indicated and shall be provided with gate stops, as specified or as shown on the Plans. Gates shall be erected at locations shown on the Plans.

161-3.8 EXISTING FENCE CONNECTIONS. Wherever the new fence joins an existing fence, either at a corner or at the intersection of straight fence lines, a corner or anchor post shall be set at the junction and braced and anchored the same as herein described for corner posts.

If the connection is made at other than the corner of the new fence, the last span of the old fence shall contain a brace span.

161-3.9 CLEANING UP. The Contractor shall remove from the vicinity of the completed work all tools, buildings, equipment, etc. used during construction.

METHOD OF MEASUREMENT

161-4.1 Fences, Class C (Steel Posts), or Class D (Steel Posts), shall be measured in place from outside to outside of end posts or corner posts and shall be the length of fence actually constructed, except for the space occupied by the gates.

161-4.2 Vehicle gates  and pedestrian gates will be measured in units for each gate installed and accepted.

BASIS OF PAYMENT

161-5.1 Payment will be made at the contract unit price per linear foot for fence and per each for gates.

Work involved in clearing and disposal of material along the fence line and any required rock excavation are subsidiary.

Payment will be made under:

Item F161.010.0010	Fence, Class C – per linear foot

Item F161.020.0020	Fence, Class D – per linear foot

Item F161.030.0003	Gates, 3-feet Wide – per each

Item F161.040.0003	Walkway Gates, 3-feet Wide – per each

MATERIAL REQUIREMENTS

AASHTO M 279	Metallic-Coated, Steel Woven Wire Fence Fabric

AASHTO M 280	Metallic-Coated (Carbon) Steel Barbed Wire

AASHTO M 181	Chain-Link Fence