## ITEM D-754	CONCRETE GUTTERS, DITCHES, AND FLUMES

DESCRIPTION

754-1.1 This item shall consist of portland cement concrete gutters, ditches, and flumes constructed according to these Specifications at the specified locations according to the dimensions, lines, and grades as shown on the Plans.

MATERIALS

754-2.1 CONCRETE. Plain and reinforced concrete shall meet the requirements of Item P-610.

754-2.2 JOINTS. Joint filler materials and premolded joint material shall conform to Item P-610.

CONSTRUCTION METHODS

754-3.1 PREPARING SUBGRADE. Excavation shall be made to the required width and depth, and the subgrade upon which the item is to be built shall be compacted to a firm uniform grade. All soft and unsuitable material shall be removed and replaced with suitable approved material. When required, a layer of approved granular material, compacted to the thickness indicated on the Plans, shall be placed to form a subbase. The underlying course shall be checked and accepted by the Engineer before placing and spreading operations are started.

754-3.2 PLACING. The forms and the mixing, placing, finishing, and curing of concrete shall conform to the requirements of Item P-610 and the following requirements.

The concrete shall be tamped until it is consolidated and mortar covers the top surface. The surface of the concrete shall be floated smooth and the edges rounded to the radii shown on the Plans. Before the concrete is given the final finishing, the surface shall be tested with a 12-foot straightedge, and any irregularities of more than 1/4 inch in 12 feet shall be eliminated.

The concrete shall be placed with dummy-grooved joints not to exceed 25 feet apart, and no section shall be less than 4 feet long.

Expansion joints of the type called for in the Plans shall be constructed to replace a dummy groove at spacings of approximately 100 feet. When the gutter is placed next to concrete pavement, expansion joints in the gutter shall be located opposite expansion joints in the pavement. When a gutter abuts a pavement or other structure, an expansion joint shall be placed between the gutter and the other structure.

Forms shall not be removed within 24 hours after the concrete has been placed. Minor defects shall be repaired with mortar containing 1 part cement and 2 parts fine aggregate.

Depositing, compacting, and finishing the item shall be conducted to build a satisfactory structure. If any section of concrete is found to be porous, or is otherwise defective, it shall be removed and replaced by the Contractor without additional compensation.

754-3.3 BACKFILLING. After the concrete has set sufficiently, the spaces adjacent to the structure shall be refilled to the required elevation with material specified on the Plans and compacted by mechanical equipment to at least 90 percent of the maximum density as determined by ATM 207 or ATM 212, except that base course for adjacent paved surfaces will be compacted as specified in Item P-209. The in-place density and moisture content shall be determined according to ATM 213.

METHOD OF MEASUREMENT

754-4.1 Concrete will be measured by the dimensions shown on the Plans or ordered by the Engineer. No deductions will be made for the volume occupied by reinforcing steel, anchors, conduits, weep holes, or piling.

754-4.2 Reinforcing steel will be measured by the theoretical weight shown on the Plans or ordered by the Engineer. No allowance will be made for clips, wire, or other material used for fastening reinforcement in place.

BASIS OF PAYMENT

754-5.1 The accepted quantities of structural concrete will be paid for at the contract unit price per cubic yard, complete in place.

754-5.2 The accepted quantities of reinforcing steel will be paid for at the contract price per pound, complete in place.

Payment will be made under:

Item D754.010.0000	Structural Concrete – per cubic yard

Item D754.020.0000	Reinforcing Steel – per pound

TESTING REQUIREMENTS

ATM 212	Standard Density of Coarse Granular Materials Using the Vibratory Compactor

ATM 207	Moisture-Density Relations of Soils

ATM 213	In-Place Density and Moisture Content of Soil and Soil-Aggregate by Nuclear Methods