## ITEM F-160	WIRE FENCE WITH WOOD POSTS (CLASS A AND B FENCES)

DESCRIPTION

160-1.1 This item covers the requirements for furnishing materials and constructing wire fences and gates with wood posts according to the details included herein and as shown on the Plans. The class of fence to be erected shall be either Class A, woven wire fencing topped by 2 strands of barbed wire, or Class B, 4 strands of barbed wire, as specified.

MATERIALS

160-2.1 WIRE.

- Woven Wire (Zinc-coated). Woven wire fabric shall meet AASHTO M 279, Design Number 726-6-12 ½, Grade 60, Coating Type Z, and Coating Class 3.

- Barbed Wire (Zinc-coated). Barbed wire shall meet AASHTO M 280, Design Number 12-4-5-14R, Standard Grade, Coating Type Z, and Coating Class 3.

- Barbed Wire (Aluminum-coated). Barbed wire shall meet AASHTO M 280, Design Number 12-4-5-14R, Standard Grade, Coating Type ZA, and Coating Class 60.

- Bracing Wire (Zinc-coated). Wire used for bracing shall be smooth galvanized wire, and shall meet AASHTO M 181, Tension Wire, except it may be 9-gage thickness.

160-2.2 GATES AND HARDWARE. Gate frames shall be constructed of hot-dip galvanized steel tubing conforming to AASHTO M 181, Type 1, Grade 1 or Grade 2, and shall be the size shown on the Plans. Heavily galvanized hinges and latches for wood posts shall be furnished with each gate. Either a bolt or lag screw hinge shall be used, and either a wing or butterfly latch shall be furnished.

160-2.3 POSTS.

- Species. All posts shall be one of the following species of wood, unless otherwise specified.

| Group I | Group II |
| --- | --- |
| Cedar | Douglas-Fir |
| Chestnut | Gum, Red |
| Cypress, Southern | Larch, Western |
| Locust, Black | Pine, Southern Yellow |
| Osage-orange | Pine, Lodgepole |
| Redwood | Tamarack |
| Yew, Pacific | Ash |
| Honey locust | Maple, Sugar |
| Oak, White | Oak, Red |
| Mulberry | Spruce |
| Live Oak |  |

- Quality. Posts shall be peeled, sound, straight-grained, and free from decay, cracks, and splits; shakes shall not be in excess of 1/4 inch wide and 3 feet long. Checks (lengthwise separations of the wood in a generally radial direction) are permitted, provided they are not harmful.

- Dimensions. All posts shall be of the length shown on the Plans. Posts shall have the minimum top diameters shown on the Plans or as specified. Sawn and split posts are acceptable instead of round posts if the required diameter round post could be turned from the sawn or split posts.

- Manufacture. Outer bark shall be completely removed from all posts including depressions. Inner bark shall be removed from all post surfaces to be treated, except inner bark may remain in depressions. The amount of wood shaved off in the removal of inner bark shall be held to a minimum.

- Treatment. Apply preservative to all timber posts. Use the preservatives and treatment processes of AASHTO M133 and Best Management Practices for the Use of Treated Wood in Aquatic Environments (BMPs), published by the Western Wood Preservers Institute, 12503 SE Mill Plain Blvd, #205 Vancouver, WA 98684 (Phone 360-693-9958). Products shall be treated according AWPA Standard U1, Commodity Specification A: Sawn Products.

160-2.4 BRACES. Cleats, gate stops, and braces shall be of the size shown on the Plans. They shall be of the same species and quality specified for the posts or approved by the Engineer, and they shall be free from knots larger than one-third the width of the piece. Gate stops shall be made of posts of suitable length. Braces may be made of posts of suitable length or of sawed lumber. All cleats, gate stops, and any braces in contact with the ground and for a distance of at least 6 inches above the ground shall be treated by the hot and cold bath process, specified herein for posts. The wire used in cable for bracing shall conform to paragraph 160-2.1e.

160-2.5 STAPLES. The staples shall be No. 9 galvanized steel wire, 1 inch long for hardwood posts and 1-1/2 inches long for use in softwood posts.

160-2.6 GATE LOCKS. Gate locks shall be provided for each gate and shall be brass, restricted keyway padlocks with a shackle that is 3/8 inch in diameter having a closed clearance of 2-1/4 inches. The locks shall have control key removable cores and each lock shall have a separate replacement core. All cores shall be keyed differently. The Contractor shall provide 4 keys per lock and 2 core removal keys.

CONSTRUCTION METHODS

160-3.1 GENERAL. The fence shall be constructed according to the details on the Plans and as specified herein. The Contractor shall be responsible for establishing the fence alignment as shown on the Plans. After the fence line has been staked and prior to fence installation, the Contractor shall review the alignment with the Engineer and make required adjustments to avoid conflicts.

When directed, the Contractor shall span the opening below the fence with barbed wire at all locations where it is not practical to conform the fence to the general contour of the ground surface because of natural or manmade features such as drainage ditches. The new fence shall be permanently tied to the terminals of existing fences whenever required by the Engineer. The finished fence shall be plumb, taut, true to line and ground contour, and complete in every detail. When directed by the Engineer, the Contractor shall stake down the woven wire fence at several points between posts.

The Contractor shall arrange the work so construction of the new fence immediately follows the removal of existing fences. The length of unfenced section at any time shall not exceed 300 feet. The work shall progress in this manner, and at the close of the working day, the newly constructed fence shall be tied to the unremoved existing fence.

160-3.2 CLEARING FENCE LINE. The site of the fence shall be sufficiently clear of obstructions, and surface irregularities shall be graded so that the fence will conform to the general contour of the ground. The fence line shall be cleared to a minimum width of 10 feet on each side of the centerline of the fence. This clearing shall consist of the removal of all stumps, brush, rocks, trees, or other obstructions that will interfere with proper construction of the fence. Stumps within the cleared area of the fence line shall be grubbed or excavated. The bottom of the fence shall be placed a uniform distance above ground as specified in the Plans. When shown on the Plans, existing fences which interfere with, the new fence location shall be removed by the Contractor as part of the construction work, unless such removal is listed as a separate item in the bid schedule. All holes remaining after post and stump removal shall be refilled with suitable soil, gravel, or other suitable material and shall be compacted with tampers.

160-3.3 SETTING POSTS. Posts shall be set with large ends down, plumb, and in a straight line on the side on which the wire is to be fastened. Posts shall be set full depth and shall not be cut off to eliminate rock or other excavation. Where rock is encountered, it shall be removed to provide full-depth and full-size holes. The bottoms of all posts shall be cut off square. The diameter of the holes shall be at least 6 inches larger than the diameter of the posts. When cleats are used on posts, the holes shall be dug large enough to accommodate them. After posts are placed and lined, the holes shall be backfilled with suitable material that shall be properly compacted by the use of tampers. The posts adjacent to end, corner, anchor, and gate posts shall be set and braced with braces and wire, as shown on the Plans.

160-3.4 ANCHORING. Corner, end, gate, and adjacent intermediate posts shall be anchored, by gaining and spiking cleats to the sides of the posts, as indicated on the Plans. No cleats will be required on other intermediate posts or on anchor posts.

160-3.5 BRACING. End, corner, anchor, and gate posts shall be braced by using a post of sufficient length or a piece of sawed lumber of the proper size, together with a wire cable. The wooden brace shall be gained and securely spiked into the end, corner, anchor, or gate posts and into the next intermediate posts about 6 inches from the top of the respective posts. A cable made of a double strand of galvanized soft wire shall be looped around the end, corner, anchor, or gate post near the ground and around the next intermediate post about 12 inches from the top. After the cable has been stapled in this position, it shall be twisted until tight. The staples used to hold the cable shall be not less than 1-1/2 inches long. The tool used for twisting the cable shall be left in placed to permit later adjustment of bracing if found necessary. Anchor posts shall be set at approximately 500-foot intervals and braced to the adjacent posts. Posts shall be braced before the wire fencing is placed.

160-3.6 INSTALLING WIRE. The wires shall be placed on the side of the posts away from the airport or as directed. The wire fence shall be placed on the posts at the height indicated on the Plans. Longitudinal wires shall be installed parallel and drawn uniformly taut. The vertical stay wires of the woven wire fencing shall be straight and vertical. At end and gate posts the woven wire and barbed wire shall be wrapped once around the post; each longitudinal wire shall be stapled at least three times and the ends of these wires shall be tied with a snug, tight twist. Each longitudinal wire shall be stapled to each intermediate post with one steel wire staple; at the corner and anchor posts, two or more stapled shall be used. The top strand of barbed wire of all fences shall be stapled with two staples in each post. All staples shall be set diagonally with the grain of the wood and driven up tight. After the fence has been erected, the tops of the wood posts shall be sawed off with a 1-to-3 pitch. The bottom wire of the wire fencing shall clear the ground by not more than 4 inches or less than 1 inch at any place.

160-3.7 SPLICING WIRE. Wire splices in longitudinal wires will be permitted if made with an approved galvanized bolt-clamp splice or a wire splice made as follows: The end of the wires shall be carried 3 inches past the splice tool and wrapped around the other wire away from the tool for at least 6 turns in opposite directions. After the tool is removed, the space occupied by it shall be closed by pulling the ends together. The unused ends of the wires shall be cut off neatly. Woven wire shall be spliced only at posts.

160-3.8 INSTALLING GATES. The gates shall be hung on gate fittings, as shown on the Plans. Fittings on the gate posts shall be clamped, screwed, or bolted to prevent slipping. Gates shall be so erected as to swing in the direction indicated and shall be provided with gate stops, as specified or as shown on the Plans. Gates shall be erected locations shown on the Plans.

160-3.9 EXISTING FENCE CONNECTIONS. Wherever the new fence joins an existing fence, either at a corner or at the intersection of straight fence lines, a corner or anchor post shall be set at the junction and braced and anchored the same as herein described for corner posts.

If the connection is made at other than the corner of the new fence, the last span of the old fence shall contain a brace span.

160-3.10 CLEANING UP. The Contractor shall remove from the vicinity of the completed work all tools, buildings, equipment, etc., used during construction.

METHOD OF MEASUREMENT

160-4.1 Fences will be measured in place from outside to outside of end posts or corner posts and will be the length of fence actually constructed, except for the space occupied by the gates.

160-4.2 Gates will be measured in units for each gate installed and accepted.

BASIS OF PAYMENT

160-5.1 Payment will be made at the contract unit price per linear foot for fence and per each for gates.

Work involved in clearing and disposal of material along the fence line and any required rock excavation are subsidiary.

Payment will be made under:

Item F160.010.0010	Fence, Class A – per linear foot

Item F160.020.0020	Fence, Class B – per linear foot

Item F160.030.____	Gates, ____-feet Wide – per each

Item F160.040.____	Walkway Gates, ____-feet Wide – per each

MATERIAL REQUIREMENTS

AASHTO M 279	Metallic-Coated, Steel Woven Wire Fence Fabric

AASHTO M 280	Metallic-Coated (Carbon) Steel Barbed Wire

AASHTO M 181	Chain-Link Fence

Fed. Spec. TT-W-571	Wood Preservation: Testing Practices