## ITEM F-162	CHAIN-LINK FENCE

DESCRIPTION

162-1.1 This item shall consist of furnishing and erecting a chain-link fence according to these specifications and the details shown on the Plans.

MATERIALS

162-2.1 FABRIC. Chain-link fabric shall meet AASHTO M 181, 9-gage thickness, Type I (zinc-coated steel), Class D coating, and 2-inch mesh.

162-2.2 BARBED WIRE. Barbed wire shall meet AASHTO M 280, Design Number 12-4-5-14R, Standard Grade, Coating Type Z, and Coating Class 3.

162-2.3 POSTS, RAILS AND BRACES. Line posts, rails, and braces shall be galvanized steel pipe, or equivalent galvanized roll-formed sections, and meet AASHTO M 181, Type I, Grade 1 or Grade 2.

The dimensions of the posts, rails, and braces shall be as shown on the Plans.

162-2.4 GATES. Gate frames shall consist of galvanized steel pipe, or equivalent galvanized roll-formed sections, and shall meet AASHTO M 181, Type I, Grade 1 or Grade 2. The fabric shall be of the same type material as used in the fence.

162-2.5 WIRE TIES AND TENSION WIRES. Wire ties for use in conjunction with a given type of fabric shall be of the same material and coating weight identified with the fabric type. Tension wire shall meet AASHTO M 181, Type I, Class 3 coating.

162-2.6 MISCELLANEOUS FITTINGS AND HARDWARE. Miscellaneous steel fittings and hardware shall meet AASHTO M 181, Type I, Grade 1 Barbed wire support arms shall withstand a load of 250 pounds applied vertically to the outermost end of the arm.

162-2.7 CONCRETE. Concrete shall be of a commercial grade with a minimum 28-day compressive strength of 2,500 pounds per square inch (psi) or an approved, pre-mixed, sacked concrete.

162-2.8 MARKING. Each roll of fabric shall carry a tag showing the kind of base metal, kind of coating, the gage of the wire, the length of fencing in the roll, and the name of the manufacturer. Posts, wire, and other fittings shall be identified as to manufacturer, kind of base metal, and kind of coating.

162-2.9 GATE LOCKS. Gate locks shall be provided for each gate and shall be brass, restricted keyway padlocks with a shackle that is 3/8 inch in diameter having a closed clearance of 2-1/4 inches. The locks shall have control key removable cores and each lock shall have a separate replacement core. All cores shall be keyed differently. The Contractor shall provide 4 keys per lock, and 2 core-removal keys.

162-2.10 KEYLESS LOCKS. When specified, a changeable combination lock shall be furnished with pedestrian gates. The keyless lock shall have a 4- or 5-digit mechanism and shall be an Ilco Unican Model 1011 or approved equal. A sign, 12 inches by 12 inches, shall be securely mounted on the inside of the gate. The sign shall be shielded from view from outside of the gate by means of a hinged 12-inch by 12-inch cover or other means approved by the Engineer. The cover shall have the legend “LIFT AND RECORD COMBINATION FOR REENTRY”. The sign shall be aluminum sheet with white reflective coating. Letters shall be black and a minimum of 3/4 inch tall.

CONSTRUCTION METHODS

162-3.1 GENERAL. The fence shall be constructed according to the details on the Plans and as specified herein using new materials. The Contractor shall be responsible for establishing the fence alignment as shown on the Plans. After the fence line has been staked and prior to fence installation, the Contractor shall review the alignment with the Engineer and make required adjustments to avoid conflicts.

The Contractor shall arrange the work so that construction of the new fence will immediately follow the removal of existing fences. The length of unfenced section at any time shall not exceed 300 feet or such length that the stock can be kept in the proper field. The work shall progress in this manner and at the close of the working day the newly constructed fence shall be tied to the existing fence.

162-3.2 CLEARING FENCE LINE. All trees, brush, stumps, logs, and other debris which would interfere with the proper construction of the fence in the required location shall be removed a minimum width of 10 feet on each side of the fence centerline before starting fencing operations.

162-3.3 INSTALLING POSTS. All end posts, corner posts and pull posts shall be set in concrete at the required dimensions and depths and at the spacing shown on the Plans. Line posts may be either set in concrete as shown on the Plans or driven a minimum of 5 feet embedment. Pull posts shall have a maximum spacing of 250 feet.

Posts shall be spaced as shown on the Plans but in no case shall spacing be more than 10 feet. The post holes shall be in proper alignment so that there is a minimum of 3 inches of concrete on all sides of the posts. The concrete shall be thoroughly compacted around the posts by tamping or vibrating and shall have a smooth finish slightly higher than the ground and sloped to drain away from the posts. All posts shall be set plumb and to the required grade and alignment. No materials shall be installed on the posts, nor shall the posts be disturbed in any manner within 7 days after the individual post footing is completed.

Should rock be encountered at a depth less than the planned embedment depth, a hole 2 inches larger than the greatest dimension of the posts shall be drilled to a depth of 12 inches. After the posts are set, the remainder of the drilled hole shall be filled with grout, composed of one part Portland cement and two parts mortar sand. Any remaining space above the rock shall be filled with concrete in the manner described above.

In lieu of drilling, the rock may be excavated to the required embedment depth.

162-3.4 INSTALLING TOP RAILS. The top rail shall be continuous and shall pass through the post tops. The coupling used to join the top rail lengths shall allow for expansion.

162-3.5 INSTALLING BRACES. Horizontal brace rails, with diagonal truss rods and turnbuckles, shall be installed at all terminal posts.

162-3.6 INSTALLING FABRIC. The wire fabric shall be firmly attached to the posts and braced in the manner shown on the Plans. All wire shall be stretched taut and shall be installed to the required elevations. The fence shall generally follow the contour of the ground, with the bottom of the fence fabric no less than 1 inch or more than 4 inches from the ground surface. Grading shall be performed where necessary to provide a neat appearance.

At locations of small natural swales or drainage ditches and where it is not practical to have the fence conform to the general contour of the ground surface, longer posts may be used and multiple strands of barbed wire stretched thereon to span the opening below the fence. The vertical clearance between strands of barbed wire shall be 6 inches or less.

162-3.7 ELECTRICAL GROUNDS. Electrical grounds shall be installed along the fence between gate openings and at intervals not exceeding 500 feet. Electrical grounds shall also be installed where a power line passes over the fence. The ground shall be accomplished with a copper clad rod 8 feet long and a minimum of 5/8 inch diameter driven vertically until the top is 6 inches below the ground surface. A No. 6 solid copper conductor shall be clamped to the rod and to the fence in such a manner that each element of the fence is grounded. The Contractor shall comply with FAA-STD-019, Lightning and Surge Protection, Grounding, Bonding and Shielding Requirements for Facilities and Electronic Equipment, Paragraph 4.2.3.8, Lightning Protection for Fences and Gates, when fencing is adjacent to FAA facilities.

162-3.8 CLEANING UP. The Contractor shall remove from the vicinity of the completed work all tools, buildings, equipment, etc., used during construction.

METHOD OF MEASUREMENT

162-4.1 Chain-link fence will be measured along the top of the fence from center to center of end posts, excluding the length occupied by gate openings.

162-4.2 Gates will be measured as complete units.

BASIS OF PAYMENT

162-5.1 Payment will be made at the contract unit price per linear foot for fence and per each for gates.

Work and materials involved in clearing and disposal of material along the fence line, rock excavation, and ground rod installation are subsidiary.

Payment will be made under:

Item F162.010.____	____-feet Chain-Link Fence – per linear foot

Item F162.030.____	Single Swing Gate, ____-feet Wide – per each

Item F162.040.____	Double Swing Gate, ____-feet Wide – per each

Item F162.050.____	Single Cantilever Gate, ____-feet Wide – per each

Item F162.060.____	Double Cantilever Gate, ____-feet Wide – per each

MATERIAL REQUIREMENTS

AASHTO M 181	Chain-Link Fence

AASHTO M 280	Metallic-Coated (Carbon) Steel Barbed Wire

ASTM A121	Standard Specification for Metallic-Coated Carbon Steel Barbed Wire

ASTM A123	Zinc (Hot Dip Galvanized) Coatings on Iron and Steel Products

ASTM A153	Zinc Coating (Hot-Dip) on Iron and Steel Hardware

ASTM A392	Zinc-Coated Steel Chain-Link Fence Fabric

ASTM A491	Aluminum-Coated Steel Chain-Link Fence Fabric

ASTM A572	High-Strength Low-Alloy Columbium-Vanadium Structural Steel

ASTM A653	Steel Sheet, Zinc-Coated (Galvanized) or Zinc-Iron Alloy-Coated (Galvannealed) by the Hot-Dip Process

ASTM A824	Metallic-Coated Steel Marcelled Tension Wire for Use With Chain Link Fence

ASTM A1011	Steel, Sheet and Strip, Hot-Rolled, Carbon, Structural, High-Strength Low-Alloy, High Strength Low Alloy with Improved Formability, and Ultra High Strength

ASTM B117	Operating Salt Spray (Fog) Apparatus

ASTM B221	Aluminum and Aluminum Alloy Extruded Bars, Rods, Wire, Profiles and Tubes

ASTM B429	Aluminum-Alloy Extruded Structural Pipe and Tube

ASTM F668	Polyvinyl Chloride(PVC) and Other Organic Polymer Coated Steel Chain-Link Fence Fabric

ASTM F1043	Strength and Protective Coatings on Steel Industrial Fence Framework

ASTM F1083	Pipe, Steel, Hot-Dipped Zinc-Coated (Galvanized) Welded, for Fence Structures

ASTM F1183	Aluminum Alloy Chain Link Fence Fabric

ASTM F1345	Zinc 5% Aluminum-Mischmetal Alloy Coated Steel Chain-Link Fence Fabric

ASTM G152	Operating Open Flame Carbon Arc Light Apparatus for Exposure of Nonmetallic Materials

ASTM G153	Operating Enclosed Carbon Arc Light Apparatus for Exposure of Nonmetallic Materials

ASTM G154 	Operating Fluorescent Ultraviolet (UV) Lamp Apparatus for Exposure of Nonmetallic Materials

ASTM G155	Operating Xenon Arc Light Apparatus for Exposure of Nonmetallic Materials

FAA-STD-019	Lighting and Surge Protection, Grounding, Bonding and Shielding Requirements for Facilities and Electronic Equipment