## ITEM F-180	SCREEN FENCE

DESCRIPTION

180-1.1 Furnish and erect a screen fence as shown on the plans.

MATERIALS

180-2.1 Provide fencing materials as shown on the plans and as follows to include zinc-coated framework, thoroughly color coated with 3-mil minimum polyester layer for protection from corrosion:

| Chain-Link Fabric: |
| --- |
| Type: | Polyvinyl chloride extruded over zinc-coated steel wire per ASTM F668 Class 1 or extruded and adhered to zinc-coated steel wire per ASTM F668 Class 2a. |
| Gauge: | 9 gauge galvanized core wire |
| Mesh: | 2 inch |
| Height: | 6 foot |
| Selvage | Knuckled top and bottom up to 5 feet high, twisted and knuckled 6 feet to 20 feet high, except 1-1/4 inch mesh and smaller knuckled top and bottom. |
| Colors: | Forest Green |
| Framework: |
| Type 2: | Spectra polyester resin, 3 mils minimum, over galvanized steel ASTM F1043, Group 1C, with a minimum yield strength of 50,000 psi. Protective coating per ASTM F1043, external coating Type B, zinc with organic overcoat, 0.9 ounces per square foot minimum zinc-coated with chromate conversion coating and verifiable polymer film. |
| Colors: | Forest Green |
| Top Rail: |
| Type 2: | 1-5/8 inch O.D. SCH 40 pipe (0.111 inch wall thickness, 1.83 lb./ft.) |
| Line Posts: |
| Type 2: | 2-3/8 inch O.D. SCH 40 pipe (0.130 inch wall thickness, 3.12 lb./ft.) |
| Terminal Posts: |
| Type 2: | 2-7/8 inch O.D. SCH 40 pipe (0.160 inch wall thickness, 4.64 lb./ft.) |
| Fittings: |
| Tension and Brace Bands: | Polymer coating, 6 mils minimum, over hot-dipped galvanized pressed steel. |
| Caps, Eye Tops, Rail Ends: | Polymer coating, 6 mils minimum, over hot-dipped galvanized pressed steel. |
| Sleeves: | Polymer coating, 6 mils minimum, over hot-dipped galvanized pressed steel. |
| Tie Wires: | Polymer coating, 6 mils minimum, over zinc-coated steel wire. |

180-2.2 CONCRETE. Provide commercial grade concrete with a minimum 28-day compressive strength of 2,500 psi or an approved, pre-mixed, sacked concrete.

CONSTRUCTION REQUIREMENTS

180-3.1 GENERAL. Construct the fence in accordance with the details shown on the plans. Establish the fence alignment as shown on the plans.

180-3.2 INSTALLING POSTS. Set all end posts, corner posts, and pull posts at the required dimensions and depths and at the spacing shown in Alaska Standard Plan F-01. Set line posts in concrete as shown on the plans.

Place posts at the intervals shown on the plans but in no case more than 10 feet apart. Thoroughly compact around the posts by tamping or vibrating. Compact backfill to a smooth surface slightly higher than the surrounding ground and sloped to drain away from the posts. Set all posts plumb and to the required grade and alignment.

METHOD OF MEASUREMENT

180-4.1 Measured along the top of the fence from center to center of end posts, excluding the length occupied by gate openings.

BASIS OF PAYMENT

180-5.1 At the contract unit price per linear foot of fence.

Work and materials involved in clearing and disposal of material along the fence line is subsidiary.

Payment will be made under:

Item F180.010.____     ____-feet Screen Fence – per linear foot