## ITEM P-161	RECYCLED ASPHALT PAVEMENT

DESCRIPTION

161-1.1 Excavate and process existing asphalt cement concrete (AC) pavement for use as Recycled Asphalt Pavement (RAP). Haul and place RAP on a prepared foundation, to the lines, grades, and depths shown on the plans or as directed by the Engineer.

MATERIAL AND CONSTRUCTION REQUIREMENTS

161-2.1 PROCESSING. Crush or pulverize existing pavement to meet the requirements of Table 161-1 for use as Recycled Asphalt Pavement (RAP). Process RAP to provide an asphalt content of 2.5 – 5.5 percent by weight.

Saw cut and process the full depth of existing pavement in areas shown on the plans or as directed by the Engineer. Excavate to the minimum depth necessary for removal of all existing pavement. Up to one inch of underlying base course material may be excavated along with the AC pavement.

TABLE 161-1

RAP GRADATION REQUIREMENTS

| Sieve Size | Percent Passing |
| --- | --- |
| 2 in. | 100 |
| 1 in. | 90-100 |

161-2.2 PLACEMENT AND SPREADING. Place RAP in 4-inch thick maximum lifts on the approved surface as required to achieve the depth shown on the plans after compaction.

Excess RAP is the property of the State. Place excess RAP in stockpiles located and shaped as shown on the plans, or as directed by the Engineer.

161-2.3 COMPACTION. Thoroughly compact the RAP layer by rolling. Density acceptance will be based on the use of a control strip in accordance with ATM 412 to determine a density standard. Compact to a density not less than 98% of the density standard. After rolling and with the RAP thoroughly set, reduce interstitial spaces to a minimum. Blade and roll alternately as required or directed to obtain a smooth, even and uniformly compacted surface. Do not roll the RAP course when the underlying course is soft or yielding or when the rolling causes undulation of the surface. In areas inaccessible to rollers, tamp RAP material thoroughly with hand held mechanical tampers.

161-2.4 RAP PROTECTION. Do not perform work on the RAP course during freezing temperatures, when the subgrade is wet, or when rain is expected. Hauling equipment may be routed over the finished RAP course, provided no damage results and provided that equipment is routed over the full width of the RAP surface to avoid rutting or uneven compaction. The Engineer has authority to stop all hauling over completed or partially completed RAP when, in his opinion, such hauling is causing damage. Repair at your expense, any damage to the RAP course resulting from the routing of equipment over RAP surfaces.

161-2.5 PROTECTION OF EXISTING STRUCTURES. Take all precautions necessary to ensure that existing structures within pavement removal areas are not damaged. If damage to any structure occurs, repair the damage at no cost to the Department.

161-2.6 DRAINAGE. Maintain drainage at all times. Install temporary drains and drainage ditches, when directed, to intercept or divert surface water that may affect the prosecution or condition of the work.

METHOD OF MEASUREMENT

161-4.1 Section 90. If RAP by unit area appears in the bid schedule, the item will be measured in original position before excavation. If RAP by unit volume appears in the bid schedule, the item will be measured in final position after processing and placement. Underlying base course material excavated along with the AC pavement will not be included in the measurement for payment of RAP measured by unit volume.

BASIS OF PAYMENT

161-5.1 At the contract unit price for recycled asphalt pavement accepted in place.

Payment will be made under:

Item P161.010.0000	Recycled Asphalt Pavement – per square yard

Item P161.020.0000	Recycled Asphalt Pavement – per cubic yard

TESTING REQUIREMENTS

ATM 412	Relative Standard Density of Treated Mixes by the Control Strip Method