## ITEM P-162	PAVEMENT COLD PLANING

DESCRIPTION

162-1.1 Cold plane existing asphalt cement concrete (AC) pavement. Clean pavement surfaces after planing. Place and shape the material produced by cold planing (millings) on a prepared foundation, to the lines, grades, and depths shown on the plans.

Excess millings are the property of the State. Place excess millings in stockpiles located and shaped as shown on the plans or as directed by the Engineer.

EQUIPMENT

162-2.1 COLD PLANING MACHINE. Use a self-propelled specialized cold planing machine with the following capabilities:

a.	Removes the millings or cuttings from the pavement surface and loads them into a truck for disposal.

- Mills the pavement to the required depth and smoothness.

- Prevents damage to any part of the remaining pavement structure.

- Establishes grade control, by string line or laser.

- Controls transverse slope.

- Mills a minimum 3-foot width of pavement per pass.

- Effectively controls dust produced during planing operations.

162-2.2 POWER BROOM. Use a self-propelled or towed power broom capable of removing all loose material resulting from the cold planing operation.

CONSTRUCTION REQUIREMENTS

162-3.1 PLANING. Furnish all materials and survey control to accomplish this work. Mill the designated areas of pavement to the depths shown on the plans. Establish any controls required to maintain the specified depth of cut or grade. Establish a finished cold-planed surface that when checked with a four-foot straight edge, does not deviate more than 3/8-inch in either the transverse or longitudinal direction.

Ensure that the cold planing operation does not adversely affect the paving schedule due to breakdowns.

162-3.2 PROTECTION OF EXISTING PAVEMENT AND STRUCTURES. Repair or replace at your expense, any pavement that is torn, cracked, gouged, broken, or undercut as directed by the Engineer. Take all precautions necessary to ensure that existing structures within pavement planing areas are not damaged. If damage to any structure occurs, repair the damage at no cost to the Department.

162-3.3 FINAL CLEANING OF COLD-PLANED SURFACES. After cold planning is complete, use a power broom to remove all loose material from the planed surface.

METHOD OF MEASUREMENT

162-4.1 Section 90. By the area of pavement in original position regardless of depth of cut, milled to the required tolerances. Placement and shaping of millings and the clean up and disposal of surplus material is subsidiary to the item.

BASIS OF PAYMENT

162-5.1 Payment will be made at the contract unit price for acceptably completed quantities.

Payment will be made under:

Item P162.010.0000	Pavement Cold Planing – per square yard