## ITEM P-180	RIPRAP

DESCRIPTION

180-1.1 Construct riprap bank and slope protection.

MATERIALS

180-2.1 Use evenly graded stones that are hard, angular, and have no more than 50% wear at 500 revolutions as determined by AASHTO T 96. Use stones with breadth and thickness at least 1/4 of its length. Do not use rounded boulders or cobbles on slopes steeper than 2:1.

Meet the following gradation for the class specified. Percents are by total weight, weights are for each stone:

Class I 	0-50% weighing up to 25 pounds

0-10% weighing more than 50 pounds

Class II 	50-100% weighing 200 pounds or more

0-15% weighing up to 25 pounds

0-10% weighing more than 400 pounds

Class III 	50-100% weighing 700 pounds or more

0-15% weighing up to 25 pounds

0-10% weighing more than 1400 pounds

Class IV 	50-100% weighing 2000 pounds or more

0-15% weighing up to 400 pounds

0-10% weighing more than 5400 pounds

CONSTRUCTION REQUIREMENTS

180-3.1 Provide a level, compact area large enough to dump and sort typical loads of riprap at approved location(s). Dump the loads specified in this area and assist the Engineer as needed to sort and measure the stones in the load to determine if the riprap is within specifications. Provide the equipment needed to assist in this sorting.

Excavate a footing trench along the toe of the slope as shown on the Plans.

Place stones to the thickness, height, and length shown on the Plans, or as staked, in a well-graded mass with a minimum of voids. Fill in unacceptable voids with smaller stones. Place riprap to its full course thickness in one operation. Avoid displacing the underlying material. Do not place riprap in layers or use methods likely to cause segregation.

Manipulate the rock sufficiently using a backhoe, rock tongs, or other suitable equipment to secure a reasonably regular surface and stability.

METHOD OF MEASUREMENT

180-4.1 Section 90. By neat line volume or by weight. Excavation and backfill will not be measured for payment and is considered subsidiary.

BASIS OF PAYMENT

180-5.1 Payment will be made at the contract unit price for each item below that appears on the bid schedule.

Payment will be made under:

Item P180.___.____	Riprap, Class ____ – per cubic yard

Item P180.___.____	Riprap, Class ____ – per ton