## ITEM P-186	SACKED SLOPE PROTECTION

DESCRIPTION

186-1.1 Furnish and place sacks (sandbags) filled with granular soils on a prepared slope as shown on the plans.

MATERIALS

186-2.1 SACKS. Provide new sacks with an approximate capacity of 1.25 cubic feet, made of at least ten ounce burlap, and measuring approximately 19-1/2 inches by 36 inches inside the seams when the sack is laid flat.

186-2.2 GRANULAR SOILS. Use granular soils for filling the sacks that meets the requirements of base course material as specified in item P-209.

186-2.3 GEOTEXTILE. Provide separation geotextile in accordance with the material requirements of specification P-681 Geotextile for Separation & Stabilization.

CONSTRUCTION REQUIREMENTS

186-3.1 Prepare slopes that are designated for sacked slope protection as shown on the plans. Repair damaged slopes where geotextile is to be placed and smoothly finish within 0.2 foot of the designated slopes. Place, join, and repair geotextile in accordance with the requirements of item P-681.

Place approximately one cubic foot of base course material in each sack. Immediately after filling, place each closed sack in position and firmly tamp to a stable condition. Conform each sack to the slope and to the adjacent sacks already in place. Prepare the excavation for toe sacks to the approximate depths and elevations shown on the plans. Place toe sacks to form a multiple row of stretchers in this prepared excavation. Prepare the next course consisting of a single row of headers. Prepare the third and remaining courses consisting of a single row of stretchers placed in such a manner that joints in succeeding courses are staggered. Remove all dirt and debris from the tops of sacks before the placing the following course. Place stretchers so that the folded ends will not be adjacent. Place headers with the folds turned in towards the bank. When, in the opinion of the Engineer, there is a lack of solid contact or there are gaps between adjacent sacks, adjust the sacks before continuing with the work.

Place two independent layers of sacked slope protection so that all joints are firm and staggered.

METHOD OF MEASUREMENT

186-4.1 Section 90. By the unit, completed and accepted in place.

BASIS OF PAYMENT

186-5.1 The accepted quantity of sacked slope protection will be paid for at the contract unit bid price per each sack, complete and in place. This price is full compensation for all materials, for preparation of slopes, for geotextiles, sacks, and base course material and for all labor, tools, equipment and incidentals for the slope protection.

Payment will be made under:

Item P186.020.0000      Sacked Slope Protection – per each