## ITEM P-189	GABIONS

DESCRIPTION

189-1.1 Construct wire gabion bank protection at locations shown on the plans.

MATERIALS

189-2.1 WIRE MESH. Use 11 gage minimum wire, except that the selvedge may be heavier. Meet or exceed ASTM A641 medium hardness and tensile strength; Class 3 coating. Furnish at least one sample of each component of the mesh for testing.

Use mesh with 4-inch openings in the longest dimension.

Use wire mesh that is designed to be nonraveling. It must resist pulling apart at any of the connections forming the mesh when a single wire strand in a section of mesh is cut.

Tie and Connecting Wire: Conform to the same specifications as wire used in the mesh except that it may be not more than 2 gauges smaller. Supply sufficient quantity for securing and fastening all edges of the gabion baskets and diaphragms, for fastening adjacent gabion baskets together, and to provide cross connecting wires in each gabion cell as specified below.

189-2.2 GABION BASKETS. Supply baskets, as specified, in various lengths and heights. Make the lengths multiples (2, 3, or more) of the horizontal width. Furnish all gabion baskets in uniform width of not less than 24 inches or more than 48 inches.

Fabricate the sides, ends, lid, and diaphragms for field assembly into a rectangular basket of the required size. Construct gabions as a unit. The base, ends and sides are either to be woven into a single unit or one edge of these members connected to the base so that strength and flexibility at the point of connection is at least equal to that of the mesh.

189-2.3 DIAPHRAGMS. Where the length of the gabion exceeds its horizontal width, divide the gabion equally with diaphragms of the same mesh and gage as the gabion basket and make compartments of a length approximately equal to horizontal width. Furnish the gabion with the necessary diaphragms secured in proper position on the base section so that no additional tying at this juncture is necessary.

Securely selvedge or bind all perimeter edges so that the joints formed by tying the selvedges have approximately the same strength as the body of the mesh.

189-2.4 GABION BACKFILL. Stone and gravel, uniformly graded from 4 to 12 inches in least dimension and having no more than 60% wear (AASHTO T 96).

CONSTRUCTION REQUIREMENTS

189-3.1 Construct gabions to the lines and grades as staked. Meet the details shown on the plans.

Assemble gabion baskets per the manufacturer's recommended procedures. Align each row or tier of gabion baskets before filling the baskets. Install tie wires in both directions horizontally so that layers between ties are not more than 14 inches thick. Space tie wires not more than 14 inches apart horizontally within any gabion basket cell. Loop tie wires around at least 3 meshes of the gabion basket and tie or twist securely. Fill each gabion basket so the lid, when secure, will bear on the gabion filler. Securely fasten gabion baskets to all adjacent baskets, using sufficient wire to provide the same strength as the body of the mesh.

Meet the requirements of section P-152 for all excavation and backfill for gabions.

METHOD OF MEASUREMENT

189-4.1 By the calculated neat line volume of gabion baskets in place using the manufacturer's specified dimensions.

BASIS OF PAYMENT

189-5.1 Excavation for gabions will be paid for under section P-152.

Payment will be made under:

Item P189.010.0000	Gabion – per cubic yard

TESTING REQUIREMENTS

AASHTO T 96	Resistance to Degradation of Small-Size Coarse Aggregate by Abrasion and Impact in the Los Angeles Machine

ASTM A641	Zinc-Coated (Galvanized) Carbon Steel Wire