## ITEM P-602	EMULSIFIED ASPHALT PRIME COAT

DESCRIPTION

602-1.1 This item shall consist of an application of liquid asphalt material on the prepared base course according to these Specifications and in reasonably close conformity to the lines shown on the Plans.

MATERIALS

602-2.1 LIQUID ASPHALT MATERIAL. The types, grades, controlling specifications, and application temperatures for the prime coat are given in Table 602-1. Provide the specific prime coat material designated in the Plans.

TABLE 602-1.    MATERIALS

| Type and Grade | Specification | Application Temperatures \1\ °F | Application Rate gal/yd2 |
| --- | --- | --- | --- |
| Emulsified Asphalt |  |  |  |
| SS-1, SS-1h | AASHTO M 140 | 70-160 | 0.27 to 0.53 |
| MS-2, HFMS-1 | AASHTO M 140 | 70-160 | 0.27 to 0.53 |
| CSS-1, CSS-1h | AASHTO M 208 | 70-160 | 0.27 to 0.53 |
| CMS-2 | AASHTO M 208 | 70-160 | 0.27 to 0.53 |
| CMS-2s | \2\ | 70-160 | 0.22 to 0.44 |
| Cutback Asphalt |  |  |  |
| RC-30 | ASTM D2028 | 80+ | 0.27 to 0.53 |
| RC-70 | ASTM D2028 | 120+ | 0.27 to 0.53 |
| RC-250 | ASTM D2028 | 165+ | 0.27 to 0.53 |
| MC-30 | ASTM D2027 | 80+ | 0.11 to 0.33 |

\1\ The maximum temperature for cutback asphalt shall be that at which fogging occurs.

\2\ CMS-2s shall meet the following specifications: Viscosity, Saybolt Furol, of 50 to 450 at 122 °F when tested under AASHTO T 59. Particle charge test of Positive when tested under AASHTO T 59. Sieve test maximum of 0.10% when tested under AASHTO T 59. Oil distillate, by volume of emulsion, of 20% maximum when tested under AASHTO T 59. Residue of 65% minimum when tested under AASHTO T 59. Penetration of 100 to 250 at 77 °F, 100 g, 5 s when tested under ASTM D5. Ductility of 40 cm minimum at 77 °F when tested under ASTM D113. Solubility in trichloroethylene of 97.5% minimum.

The Contractor shall provide samples of the prime coat material and a copy of the manufacturer’s Certificate of Analysis (COA) for each carload or equivalent of the liquid asphalt material to the Engineer for review and acceptance before the liquid asphalt material is applied. The furnishing of the COA for the liquid asphalt material shall not be interpreted as a basis for final acceptance.  The manufacturer’s COA may be subject to verification by testing the material delivered for use on the project.

CONSTRUCTION METHODS

602-3.1 WEATHER LIMITATIONS. The prime coat shall be applied only when the existing surface is dry or contains sufficient moisture to get uniform distribution, when the surface temperature is above 45 °F, and when the weather is not foggy or rainy. The temperature requirements may be waived, but only when so directed by the Engineer.

602-3.2 EQUIPMENT. The equipment used by the Contractor shall include a self-powered pressure distributor and equipment for heating the prime coat.

The distributor shall be designed, equipped, maintained, calibrated within the past year to ASTM D2995, and operated so that prime coat at even heat may be applied uniformly on variable widths of surface at the specified rate. The allowable variation from the specified rate shall not exceed 5%. Distributor equipment shall include a tachometer, pressure gages, volume-measuring devices or a calibrated tank, and a thermometer for measuring temperatures of tank contents. The distributor shall be self-powered and shall be equipped with a power unit for the pump and full circulation spray bars adjustable laterally and vertically.

A power broom and/or blower shall be provided for any required cleaning of the surface to be treated.

602-3.3 APPLICATION OF PRIME COAT. Immediately before applying the prime coat, the full width of the surface to be primed shall be swept with a power broom to remove all loose dirt and other objectionable material.

The prime coat including solvent shall be uniformly applied with an asphalt distributor at the rate specified in Table 602-1, depending on the base course surface texture. The type of liquid asphalt material and application rate shall be approved by the Engineer prior to application.

Following the application, the primed surface shall be allowed to cure not less than 48 hours without being disturbed or for such additional time as may be necessary to permit the drying out of the prime until it will not be picked up by traffic or equipment. This period shall be determined by the Engineer. The surface shall then be maintained by the Contractor until the surfacing has been placed. Suitable precautions shall be taken by the Contractor to protect the primed surface against damage during this interval, including supplying, spreading, and removing any sand necessary to blot up excess prime coat.

602-3.4 TRIAL APPLICATION RATES. The Contractor shall conduct a trial application in the presence of the Engineer to demonstrate the liquid asphalt material can be satisfactorily applied within the application range specified in Table 602-1 for the specified material.

602-3.5 FREIGHT AND WAYBILLS. Before the final estimate is allowed, the Contractor shall file with the Engineer receipted bills when railroad shipments are made, and certified waybills when materials are received in any other manner, of the prime coat actually used in the construction covered by the contract. The Contractor shall not remove prime coat from the tank car or storage tank until the initial outage and temperature measurements have been taken by the Engineer, nor shall the car or tank be released until the final outage has been taken by the Engineer.

Copies of freight bills and waybills shall be furnished to the Engineer during the progress of the work.

METHOD OF MEASUREMENT

602-4.1 Prime coat will be measured by the ton, according to Subsection GCP-90-02.  Removing any sand necessary to blot up excess prime coat is subsidiary to the work.  Water added to emulsified asphalt will not be measured for payment.

BASIS OF PAYMENT

602-5.1 Payment will be made at the contract unit price per ton for accepted prime coat.

Payment will be made under:

Item P602.010.____	Prime Coat, _____ – per ton

TESTING REQUIREMENTS

AASHTO T59	Test for Emulsified Asphalts

ASTM D5	Penetration of Bituminous Materials

ASTM D113	Ductility of Asphalt Materials

ASTM D2995	Estimating Application Rate and Residual Application Rate of Bituminous Distributors

MATERIAL REQUIREMENTS

AASHTO M140	Emulsified Asphalt

AASHTO M208	Cationic Emulsified Asphalt

ASTM D2027	Cutback Asphalt (Medium-Curing Type)

ASTM D2028	Cutback Asphalt (Rapid Curing Type)