## ITEM P-605	JOINT SEALANTS FOR PAVEMENTS

DESCRIPTION

605-1.1 This item shall consist of providing and installing a resilient and adhesive joint sealing material capable of effectively sealing joints in pavement; joints between different types of pavements; and cracks in existing pavement.

MATERIALS

605-2.1 JOINT SEALANTS. Joint sealing material shall meet the requirements of ASTM D6690 for sealing joints or cracks in Asphalt or Portland Cement Concrete Pavements.  Joint sealing material shall meet the requirements of ASTM D7116 for sealing joints or cracks in Portland Cement Concrete Pavements only where fueling occurs.

Each lot or batch of sealing compound shall be delivered to the jobsite in the manufacturer's original sealed container. Each container shall be marked with the manufacturer's name, batch or lot number, and the safe heating temperature, and shall be accompanied by the manufacturer's certification stating that the compound meets the requirements of this specification.

605-2.2 BACKER ROD. The material furnished shall be a compressible, non-shrinking, non-staining, non-absorbing material that is non-reactive with the joint sealant in accordance with ASTM D5249.  The backer-rod material shall be 25% ± 5 % larger in diameter than the nominal width of the joint.

605-2.3 BOND BREAKING TAPES. Provide a bond breaking tape, or separating material that is a flexible, non-shrinkable, non-absorbing, non-staining, and non-reacting adhesive-backed tape. The material shall have a melting point at least 5°F greater than the pouring temperature of the sealant being used when tested in accordance with ASTM D789. The bond breaker tape shall be approximately 1/8 inch wider than the nominal width of the joint and shall not bond to the joint sealant.

605-2.4 BACKUP MATERIAL. Provide backup material that is a compressible, non-shrinking, non-staining, non-absorbing material, nonreactive with the joint sealant. The material shall have a melting point at least 5°F greater than the pouring temperature of the sealant being used when tested in accordance with ASTM D789. The material shall have a water absorption of not more than 5% of the sample weight when tested in accordance with ASTM C509. The backup material shall be 25 ±5% larger in diameter than the nominal width of the crack.

CONSTRUCTION METHODS

605-3.1 TIME OF APPLICATION. Joints shall be sealed as soon after completion of the curing period as feasible and before the pavement is opened to traffic, including construction equipment. The pavement temperature shall be above 50 °F and rising at the time of installation of the poured joint sealing material. Do not apply sealant if moisture is observed in the joint.

605-3.2 EQUIPMENT. Machines, tools, and equipment used in the performance of the work required by this section shall be approved before the work is started and maintained in satisfactory condition at all times. Submit a list of proposed equipment to be used in performance of construction work including descriptive data, at least 15 days prior to use on the project.

- Tractor-mounted routing tool. Provide a routing tool, used for removing old sealant from the joints, of such shape and dimensions and so mounted on the tractor that it will not damage the sides of the joints. The tool shall be designed so that it can be adjusted to remove the old material to varying depths as required. The use of V-shaped tools or rotary impact routing devices will not be permitted. Hand-operated spindle routing devices may be used to clean and enlarge random cracks.

- Concrete saw. Provide a self-propelled power saw, with water-cooled diamond or abrasive saw blades, for cutting joints to the depths and widths specified.

- Sandblasting equipment. The Contractor must demonstrate sandblasting equipment including the air compressor, hose, guide, and nozzle size, under job conditions, before approval in accordance with subsection 605-3.3. The Contractor shall demonstrate, in the presence of the Engineer, that the method cleans the joint and does not damage the joint.

- Waterblasting equipment.  The Contractor must demonstrate waterblasting equipment including the pumps, hose, guide, and nozzle size, under job conditions, before approval in accordance with subsection 605-3.3. The Contractor shall demonstrate, in the presence of the Engineer, that the method cleans the joint and does not damage the joint.

- Hand tools.  Hand tools may be used, when approved, for removing defective sealant from a crack and repairing or cleaning the crack faces. Hand tools should be carefully evaluated for potential spalling effects prior to approval for use.

- Hot-poured sealing equipment. The unit applicators used for heating and installing ASTM D6690 joint sealant materials shall be mobile and shall be equipped with a double-boiler, agitator-type kettle with an oil medium in the outer space for heat transfer; a direct-connected pressure-type extruding device with a nozzle shaped for inserting in the joint to be filled; positive temperature devices for controlling the temperature of the transfer oil and sealant; and a recording type thermometer for indicating the temperature of the sealant. The applicator unit shall be designed so that the sealant will circulate through the delivery hose and return to the inner kettle when not in use.

- Cold-applied, single-component sealing equipment. The equipment for installing ASTM D5893 single component joint sealants shall consist of an extrusion pump, air compressor, following plate, hoses, and nozzle for transferring the sealant from the storage container into the joint opening. The dimension of the nozzle shall be such that the tip of the nozzle will extend into the joint to allow sealing from the bottom of the joint to the top. Maintain the initially approved equipment in good working condition, serviced in accordance with the supplier’s instructions, and unaltered in any way without obtaining prior approval. Small hand-held air-powered equipment (i.e., caulking guns) may be used for small applications.

605-3.3 PREPARATION OF JOINTS.  Pavement joints for application of material in this specification must be dry, clean of all scale, dirt, dust, curing compound, and other foreign matter.  Demonstrate, in the presence of the Engineer, that the method cleans the joint and does not damage the joint.

- Sawing. All joints shall be sawed in accordance with specifications and plan details. Immediately after sawing the joint, the resulting slurry shall be completely removed from joint and adjacent area by flushing with a jet of water, and by use of other tools as necessary.

- Sealing. Immediately before sealing, the joints shall be thoroughly cleaned of all laitance, curing compound, filler, protrusions of hardened concrete, old sealant and other foreign material from the sides and upper edges of the joint space to be sealed. Cleaning shall be accomplished by tractor-mounted routing equipment, concrete saw, sandblasting (if permitted), waterblasting, or by wire brushing. Upon completion of cleaning, the joints shall be blown out with compressed air. The joint faces shall be surface dry when the seal is applied.

- Backer Rod. When the joint opening is of a greater depth than indicated for the sealant depth, plug or seal off the lower portion of the joint opening using a backer rod or backup material to prevent the entrance of the sealant below the specified depth. Take care to ensure that the backer rod or backup material is placed at the specified depth and is not stretched or twisted during installation.

- Bond-breaking tape. Where inserts or filler materials contain bitumen, or the depth of the joint opening does not allow for the use of a backup material, insert a bond-breaker separating tape to prevent incompatibility with the filler materials and three-sided adhesion of the sealant. Securely bond the tape to the bottom of the joint opening so it will not float up into the new sealant.

Prior to resealing joints, the existing joint sealant shall be removed to the depth as shown on the Plans. If joint sealant other than that originally used is specified, all existing joint sealant shall be removed.

605-3.4 INSTALLATION OF SEALANT. Joints shall be inspected for proper width, depth, alignment, and preparation, and shall be approved by the Engineer before sealing is allowed.

Perform a final cleaning with compressed air not more than 50 feet ahead of the joint sealing operations. Fill the joints from the bottom up to 1/8 inch ±1/16 inch below the top of pavement surface; or bottom of groove for grooved pavement. Remove and discard excess or spilled sealant from the pavement by approved methods. Install the sealant in such a manner as to prevent the formation of voids and entrapped air. In no case shall gravity methods or pouring pots be used to install the sealant material. Traffic shall not be permitted over newly sealed pavement until authorized by the Engineer. When a primer is recommended by the manufacturer, apply it evenly to the joint faces in accordance with the manufacturer’s instructions. Check the joints frequently to ensure that the newly installed sealant is cured to a tack-free condition within the time specified.

The joint sealant shall be applied uniformly solid from bottom to top and shall be filled without formation of entrapped air or voids. Backer rod or backup material shall be placed as shown on the Plans and shall be non-adhesive to the concrete or the sealant material. The heating kettle shall be an indirect heating type, constructed as a double boiler. A positive temperature control and mechanical agitation shall be provided. The sealant shall not be heated to within 20°F below the safe heating temperature. The safe heating temperature can be obtained from the manufacturer's shipping container. A direct connecting pressure type extruding device with nozzles shaped for insertion into the joint shall be provided. Any sealant spilled on the surface of the pavement shall be removed immediately.

605-3.5 INSPECTION. The Contractor shall inspect the joint sealant for proper rate of cure and set, bonding to the joint walls, cohesive separation within the sealant, reversion or return to liquid, entrapped air and voids. Sealants exhibiting any of these deficiencies at any time prior to the final acceptance of the project shall be removed from the joint, wasted, and replaced as specified at no additional cost to the Department.

605-3.6 CLEAN-UP. Upon completion of the project, remove all unused materials from the site and leave the pavement in a clean condition.

METHOD OF MEASUREMENT

605-4.1 Joint sealing material will be measured by the linear foot of sealant in place, complete, and accepted.

BASIS OF PAYMENT

605-5.1 Payment for joint sealing material will be made at the contract unit price per linear foot, and according to GCP Section 90.

Payment will be made under:

Item P605.010.0000	Joint Sealing Filler – per linear foot

TESTING REQUIREMENTS

ASTM D789	Determination of Relative Viscosity of Concentrated Polyamide (PA) Solutions

MATERIAL REQUIREMENTS

ASTM C509	Elastomeric Cellular Preformed Gasket and Sealing Material

ASTM D5249	Backer Material for Use with Cold- and Hot-Applied Joint Sealants in Portland-Cement Concrete and Asphalt Joints

ASTM D5893 	Cold Applied, Single Component, Chemically Curing Silicone Joint Sealant for Portland Cement Concrete Pavements

ASTM D6690	Joint and Crack Sealants, Hot Applied, for Concrete and Asphalt Pavements

ASTM D7116	Joint Sealants, Hot Applied, Jet Fuel Resistant Types, for Portland Cement Concrete Pavements