## ITEM P-606	ADHESIVE COMPOUNDS, TWO-COMPONENT 
FOR SEALING WIRE AND LIGHTS IN PAVEMENT

DESCRIPTION

606-1.1 This specification covers two types of material: a liquid suitable for sealing electrical wire in saw cuts in pavement and sealing light fixtures or bases in pavement; a paste suitable for embedding light fixtures and aircraft tie-downs in the pavement. Both types of material are two-component filled formulas with the characteristics specified in Subsection 606-2.4. Materials supplied for use with asphalt and/or concrete pavements must be formulated so they are compatible with the asphalt and/or concrete.

EQUIPMENT AND MATERIALS

606-2.1 CURING. When pre-warmed to 77°F, mixed, and placed according to manufacturer's directions, the materials shall cure at temperatures of 45°F or above without the application of external heat.

606-2.2 STORAGE. The adhesive components shall not be stored at temperatures over 86°F, unless otherwise specified by the manufacturer.

606-2.3 CAUTION. Installation and use shall be according to the manufacturer's recommended procedures. Avoid prolonged or repeated contact with skin. In case of contact, wash with soap and flush with water. If taken internally, call doctor. Keep away from heat or flame. Avoid vapor. Use in well-ventilated areas. Keep in cool place. Keep away from children.

606-2.4 CHARACTERISTICS. When mixed and cured according to the manufacturer's directions, the materials shall have the following properties shown in Table 606-1.

TABLE 606-1.    PROPERTY REQUIREMENTS

| Physical or Electrical Property | Minimum | Maximum | ASTM Method |
| --- | --- | --- | --- |
| Tensile |  |  |  |
| Portland Cement Concrete | 1,000 psi |  | D638 |
| Asphalt Concrete | 500 psi |  |  |
| Elongation |  |  |  |
| Portland Cement Concrete | 8% \1\ |  | D638 |
| Hot Mix Asphalt | 50% |  | D638 |
| Coef. of cub. exp., cm3/cm3/°C | 0.00090 | 0.00120 | D1168-08 |
| Coef. of lin. exp., cm/cm/°C | 0.00030 | 0.00040 | D1168-08 |
| Dielectric strength, short time test | 350 volts/mil. |  | D149 |
| Arc resistance | 125 secs. |  | D495 |
| Pull-off |  |  |  |
| Adhesion to steel | 1,000 psi |  |  |
| Adhesion to Portland cement concrete | 200 psi |  |  |
| Adhesion to asphalt concrete | (no test available) |  |  |
| Adhesion to aluminum | 250 psi |  |  |

\1\ 20% or more (without filler) for formulations to be supplied for areas subject to freezing.

SAMPLING, INSPECTION, AND TEST PROCEDURES

606-3.1 TENSILE PROPERTIES. Tests for tensile strength and elongation shall be conducted according to ASTM D638.

606-3.2 EXPANSION. Tests for coefficients of linear and cubical expansion shall be conducted according to ASTM D1168-08, Method B, except that mercury shall be used instead of glycerin. The test specimen(s) shall be mixed in the proportions specified by the manufacturer, and cured in a glass tube approximately 2 inches long by 3/8 inch in diameter. The interior of the tube shall be precoated with a silicone mold release agent. The hardened sample shall be removed from the tube and aged at room temperature for 1 week before conducting the test. The test temperature range shall be from 35°F to 140°F.

606-3.3 TEST FOR DIELECTRIC STRENGTH. Test for dielectric strength shall be conducted according to ASTM D149 for sealing compounds to be furnished for sealing electrical wires in pavement.

606-3.4 TEST FOR ARC RESISTANCE. Test for arc resistance shall be conducted according to ASTM D495 for sealing compounds to be furnished for sealing electrical wires in pavement.

606-3.5 TEST FOR ADHESION TO STEEL. The ends of two smooth, clean, steel specimens (approximately 1-inch by 1-inch by 6 inches) are bonded together with adhesive mixture and allowed to cure at room temperature for a period of time to meet formulation requirements and then tested to failure on a Riehle (or similar) tensile tester. The thickness of adhesive to be tested shall be 1/4-inch.

606-3.6 ADHESION TO PORTLAND CEMENT CONCRETE.

- Concrete Test Block Preparation. The aggregate grading shall be as shown in Table 606-2. The coarse aggregate shall consist of crushed rock having a minimum of 75% of the particles with at least one fractured face and having a water absorption of not more than 1.5%. The fine aggregate shall consist of crushed sand manufactured from the same parent rock as the coarse aggregate. The concrete shall have a water-cement ratio of 5.5 gallons of water per bag of cement, a cement factor of 6, plus or minus 0.5, bags of cement per cubic yard of concrete, and a slump of 2-1/2 inches plus or minus 1/2 inch. The ratio of fine aggregate to total aggregate shall be approximately 40% by solid volume. The air content shall be 5.0%, plus or minus 0.5%, and it shall be obtained by the addition to the batch of an air-entraining admixture such as Vinsol® resin. The mold shall be metal with a metal base plate.

Means shall be provided for securing the base plate to the mold. The assembled mold and base plate shall be watertight and shall be oiled with mineral oil before use. The inside measurement of the mold shall be such that several 1-inch by 2-inch by 3-inch test blocks can be cut from the specimen with a concrete saw having a diamond blade. The concrete shall be prepared and cured according to AASHTO R 39.

TABLE 606-2.    AGGREGATE FOR BOND TEST BLOCKS

| Type | Sieve Size | Percent Passing |
| --- | --- | --- |
| Coarse Aggregate | 3/4 in. | 97 to 100 |
|  | 1/2 in. | 63 to 69 |
|  | 3/8 in. | 30 to 36 |
|  | No. 4 | 0 to 3 |
| Fine Aggregate | No. 4 | 100 |
|  | No. 8 | 82 to 88 |
|  | No. 16 | 60 to 70 |
|  | No. 30 | 40 to 50 |
|  | No. 50 | 16 to 26 |
|  | No. 100 | 5 to 9 |

- Bond Test. Prior to use, oven-dry the test blocks to constant weight at a temperature of 220 to 230°F, cool to room temperature, 73.4 ±3°F, in a desiccator, and clean the surface of the blocks of film or powder by vigorous brushing with a stiff-bristled fiber brush. Two test blocks shall be bonded together on the 1-inch by 3-inch sawed face with the adhesive mixture and allowed to cure at room temperature for a period of time to meet formulation requirements and then tested to failure in a Riehle (or similar) tensile tester. The thickness of the adhesive to be tested shall be 1/4 inch.

606-3.7 COMPATIBILITY WITH ASPHALT MIX. Test for compatibility with asphalt according to ASTM D5329.

606-3.8 CERTIFICATION. The Contractor shall furnish the vendor's certified test reports for each batch of material delivered to the project. The report shall certify that the material meets specification requirements and is suitable for use with Portland cement concrete or asphalt concrete pavements. The report shall be provided to and accepted by the Engineer before use of the material. In addition the Contractor shall obtain a statement from the supplier or manufacturer which guarantees the material for one year. The supplier or manufacturer shall furnish evidence that the material has performed satisfactorily on other projects.

606-3.9 APPLICATION. Adhesive shall be applied on a dry, clean surface, free of grease, dust, and other loose particles. The method of mixing and application shall be in strict accordance with the manufacturer's recommendations. When used with Item P-605, such as light can installation, Item P-605 shall not be applied until Item P-606 has fully cured.

METHOD OF MEASUREMENT

606-4.1 The adhesive compound will be measured according to GCP Section90 and by the pound of adhesive as specified, in place, complete and accepted with the following exceptions. When required in the installation of an in-runway lighting system, taxiway lighting system or portion thereof, or for aircraft tie-down, no measurement will be made for direct payment of adhesive, as the cost of furnishing and installing will be considered as a subsidiary obligation in the completion of the installation.

BASIS OF PAYMENT

606-5.1 Payment will be made, where applicable, at the contract unit price per pound for the adhesive. If the following pay item is absent from the bid schedule, no payment will be made.

Payment will be made under:

Item P606.010.0000	Adhesive Compound – per pound

TESTING REQUIREMENTS

AASHTO R 39	Making and Curing Concrete Test Specimens in the Laboratory

ASTM D149	Dielectric Breakdown Voltage and Dielectric Strength of Solid Electrical Insulating Materials at Commercial Power Frequencies

ASTM D495	High-Voltage, Low-Current, Dry Arc Resistance of Solid Electrical Insulation

ASTM D638	Tensile Properties of Plastics

ASTM D1168-08	Hydrocarbon Waxes Used for Electrical Insulation

ASTM D5329	Sealants and Fillers, Hot-Applied, for Joints and Cracks in Asphalt Pavements and Portland Cement Concrete Pavements