## ITEM P-610	CONCRETE FOR MISCELLANEOUS STRUCTURES

DESCRIPTION

610-1.1 This item shall consist of concrete and reinforcement, as shown on the plans, prepared and constructed in accordance with these Specifications. This specification shall be used for all concrete other than airfield pavement which are cast-in-place.

MATERIALS

610-2.1 GENERAL. Only approved materials, conforming to the requirements of these Specifications, shall be used in the work. Materials may be subject to inspection and tests at any time during their preparation or use. The source of all materials shall be approved by the Engineer before delivery or use in the work. Representative preliminary samples of the materials shall be submitted by the Contractor, when required, for examination and test. Materials shall be stored and handled to ensure preservation of their quality and fitness for use and shall be located to facilitate prompt inspection. All equipment for handling and transporting materials and concrete must be clean before any material or concrete is placed in them.

The use of pit-run aggregates shall not be permitted unless the pit-run aggregate has been screened and washed, and all fine and coarse aggregates stored separately and kept clean. The mixing of different aggregates from different sources in one storage stockpile or alternating batches of different aggregates shall not be permitted.

- Reactivity. Fine aggregate and coarse aggregates to be used in all concrete shall have been tested separately within six months of the project in accordance with ASTM C1260.  Test results shall be submitted to the Engineer. The aggregate shall be considered innocuous if the expansion of test specimens, tested in accordance with ASTM C1260, does not exceed 0.08% at 14 days (16 days from casting).  If the expansion either or both test specimen is greater than 0.08% at 14 days, but less than 0.20%, a minimum of 25% of Type F fly ash, or between 40% and 55% of slag cement shall be used in the concrete mix.

If the expansion is greater than 0.20%, the aggregates shall not be used, and test results for other aggregates must be submitted for evaluation; or aggregates that meet P-501 reactivity test requirements may be utilized.

610-2.2 COARSE AGGREGATE. The coarse aggregate for concrete shall meet the requirements of AASHTO M 80, Class A.

Coarse aggregate shall be well graded from coarse to fine, and shall meet AASHTO M 43, Number 57 or 67, when tested according to ATM 304.

610-2.2.1 COARSE AGGREGATE SUSCEPTIBILITY TO DURABILITY (D) CRACKING.  Not Used.

610-2.3 FINE AGGREGATE. The fine aggregate for concrete shall meet all fine aggregate requirements of AASHTO M 6, Class A.

610-2.4 CEMENT. Cement shall conform to the requirements of AASHTO M 85.

610-2.5 CEMENTITIOUS MATERIALS.

- Fly ash. Fly ash shall meet the requirements of AASHTO M 295, with the exception of loss of ignition, where the maximum shall be less than 6%. Fly ash shall have a Calcium Oxide (CaO) content of less than 15% and a total available alkali content less than 3% per AASHTO M 295.  Fly ash produced in furnace operations using liming materials or soda ash (sodium carbonate) as an additive shall not be acceptable. The Contractor shall furnish the previous three most recent, consecutive AASHTO M 295 reports for each source of fly ash proposed in the concrete mix, and shall furnish each additional report as they become available during the project. The reports can be used for acceptance or the material may be tested independently by the Engineer.

- Slag cement (ground granulated blast furnace (GGBF)).  Slag cement shall conform to AASHTO M 302, Grade 100 or Grade 120. Slag cement shall be used only at a rate between 25% and 55% of the total cementitious material by mass.

610-2.6 WATER. Water used in mixing or curing shall be from potable water sources. Water from ‘Community’ or ‘Non-Transient Non-Community’ sources regulated by the Alaska Department of Environmental Conservation Division of Environmental Health Drinking Water Program, or equivalent in other states, do not require testing under ASTM C1602. Other sources shall be tested in accordance with ASTM C1602 prior to use.

610-2.7 ADMIXTURES. The Contractor shall submit certificates indicating that the material to be furnished meets all of the requirements indicated below. In addition, the Engineer may require the Contractor to submit complete test data from an approved laboratory showing that the material to be furnished meets all of the requirements of the cited specifications. Subsequent tests may be made of samples taken by the Engineer from the supply of the material being furnished or proposed for use on the work to determine whether the admixture is uniform in quality with that approved.

- Air-entraining admixtures. Air-entraining admixtures shall meet the requirements of AASHTO M 154 and shall consistently entrain the air content in the specified ranges under field conditions. The air-entrainment agent and any water reducer admixture shall be compatible.

- Water-reducing admixtures.  Water-reducing admixture shall meet the requirements of AASHTO M 194, Type A, B, or D. AASHTO M 194, Type F and G high range water reducing admixtures and ASTM C1017 flowable admixtures shall not be used.  Water-reducing admixtures shall be added at the mixer separately from air-entraining admixtures according to the manufacturer's printed instructions.

- Other chemical admixtures. The use of set retarding, and set-accelerating admixtures shall be approved by the Engineer.  Retarding shall meet the requirements of AASHTO M 194, Type A, B, or D and set-accelerating shall meet the requirements of AASHTO M 194, Type C.  Calcium chloride and admixtures containing calcium chloride shall not be used.

610-2.8 PREMOLDED JOINT MATERIAL. Premolded joint material for expansion joints shall meet the requirements of AASHTO M 213.

610-2.9 JOINT FILLER. The filler for joints shall meet the requirements of Item P-605.

610-2.10 STEEL REINFORCEMENT. Reinforcing shall consist of Deformed and Plain Carbon-Steel Bars conforming to the requirements of ASTM A615, Welded Steel Wire Fabric conforming to the requirements of ASTM A1064, Welded Deformed Steel Fabric conforming to the requirements of ASTM A1064, or Bar Mats conforming to the requirements of ASTM A184, as shown on the Plans.

610-2.11 MATERIALS FOR CURING CONCRETE. Curing materials shall conform to Table 610-1:

TABLE 610-1. MATERIALS FOR CURING CONCRETE

| CURING MATERIAL | SPECIFICATION |
| --- | --- |
| Burlap Cloth made from Jute or Kenaf and Cotton Mats | AASHTO M 182, Class 4 |
| Sheet Materials for Curing Concrete | ASTM C171 |
| Liquid Membrane – Forming Compounds for Curing Concrete | ASTM C309, Type 1-D Class B, except do not use compounds containing linseed oil. |

CONSTRUCTION METHODS

610-3.1 GENERAL. The Contractor shall furnish all labor, materials, and services necessary for, and incidental to, the completion of all work as shown on the drawings and specified here. All machinery and equipment used by the Contractor on the work, shall be of sufficient size to meet the requirements of the work. All work shall be subject to the inspection and approval of the Engineer.

610-3.2 CONCRETE MIXTURE. The concrete shall develop a minimum compressive strength of 4,000 psi in 28 days as determined by test cylinders made according to ATM 506 and tested according to AASHTO T 22. The concrete shall contain not less than 470 pounds of cementitious material per cubic yard.  The concrete shall contain 5.0% of entrained air, plus or minus 1.2%, as determined by ATM 505. Slump, as determined by ATM 503, shall match the mix design target value plus or minus 1 inch.

610-3.3 MIXING. Concrete may be mixed at the construction site, at a central point, or wholly or in part in truck mixers. The concrete shall be mixed and delivered in accordance with the requirements of AASHTO M 157.

The concrete shall be mixed only in quantities required for immediate use. Concrete shall not be mixed while the air temperature is below 40°F without the Engineer’s approval. If approval is granted for mixing under such conditions, aggregates or water, or both, shall be heated and the concrete shall be placed at a temperature not less than 50°F nor more than 100°F. The Contractor shall be held responsible for any defective work, resulting from freezing or injury in any manner during placing and curing, and shall replace such work at his expense.

Retempering of concrete by adding water or any other material is not permitted.

The rate of delivery of concrete to the job shall be sufficient to allow uninterrupted placement of the concrete.

610-3.4 FORMS. Concrete shall not be placed until all the forms and reinforcements have been inspected and approved by the Engineer. Forms shall be of suitable material and shall be of the type, size, shape, quality, and strength to build the structure as shown on the Plans. The forms shall be true to line and grade and shall be mortar-tight and sufficiently rigid to prevent displacement and sagging between supports. The surfaces of forms shall be smooth and free from irregularities, dents, sags, and holes. The Contractor shall be responsible for their adequacy.

The internal form ties shall be arranged so that no metal will show in the concrete surface or discolor the surface when exposed to weathering when the forms are removed. All forms shall be wetted with water or with a non-staining mineral oil, which shall be applied immediately before the concrete is placed. Forms shall be constructed so they can be removed without injuring the concrete or concrete surface.

610-3.5 PLACING REINFORCEMENT. All reinforcement shall be accurately placed, as shown on the Plans, and shall be firmly held in position during concrete placement. Bars shall be fastened together at intersections. The reinforcement shall be supported by approved metal chairs. Shop drawings, lists, and bending details shall be supplied by the Contractor when required.

Reinforcing bars shall be bent cold and shall conform accurately to the shape and dimensions shown on the diagram. In no case shall the radius of any bend be less than 4 times the diameter of the bar.

Place reinforcement as indicated on the Plans or as hereinafter specified. Rigidly block and wire in place, using metal or plastic supports or concrete blocks and securely tie at each intersection with annealed iron wire of at least 1/8 inch.

Do not splice bars at points not indicated on the Plans except with the consent of the Engineer. Such splices shall be at the points of minimum tensile stress and the lap shall be not less than 36 bar diameters.

Verify the quantity, size, and shape of the reinforcement against the structure drawings and make necessary corrections to the bar lists and bending schedules before ordering. Errors in the bar lists and/or bending schedules shall not be cause for adjustment of the contract prices.

If reinforcing bars are to be welded, follow AWS D12.1.

610-3.6 EMBEDDED ITEMS. Before placing concrete, all embedded items shall be firmly and securely fastened in place as indicated. All embedded items shall be clean and free from coating, rust, scale, oil, or any foreign matter. The concrete shall be spaded and consolidated around and against embedded items. The embedding of wood shall not be allowed.

610-3.7 CONCRETE CONSISTENCY. The Contractor shall monitor the consistency of the concrete delivered to the project site; collect each batch ticket; check temperature; and perform slump tests on each truck at the project site in accordance with ATM 503.

610-3.8 PLACING CONCRETE. All concrete shall be placed during daylight hours, unless otherwise approved. The concrete shall not be placed until the depth and condition of foundations, the adequacy of forms and falsework, and the placing of the steel reinforcing have been approved by the Engineer. Concrete shall be placed as soon as practical after mixing, but in no case later than one (1) hour after water has been added to the mix. The method and manner of placing shall avoid segregation and displacement of the reinforcement. Troughs, pipes, and chutes shall be used as an aid in placing concrete when necessary. The concrete shall not be dropped from a height of more than 5 feet. Concrete shall be deposited as nearly as practical in its final position to avoid segregation due to rehandling or flowing. Do not subject concrete to procedures which cause segregation. Concrete shall be placed on clean, damp surfaces, free from running water, or on a properly consolidated soil foundation.

610-3.9 VIBRATION.  Vibration shall follow the guidelines in American Concrete Institute (ACI) Committee 309R, Guide for Consolidation of Concrete.

610-3.10 JOINTS. Joints shall be constructed as indicated on the plans.

610-3.11 FINISHING. All exposed concrete surfaces shall be true, smooth, and free from open or rough areas, depressions, or projections. All concrete horizontal plane surfaces shall be brought flush to the proper elevation with the finished top surface struck-off with a straightedge and floated.

610-3.12 CURING AND PROTECTION. All concrete shall be properly cured in accordance with the recommendations in American Concrete Institute (ACI) 308R, Guide to External Curing of Concrete.  The concrete shall be protected from damage until project acceptance.

610-3.13 COLD WEATHER PLACING. When concrete is placed at temperatures below 40°F, follow the cold weather concreting recommendations found in ACI 306R, Cold Weather Concreting.

610-3.14 HOT WEATHER PLACING. When concrete is placed at temperatures greater than 85ºF, follow the hot weather concreting recommendations found in ACI 305R, Hot Weather Concreting.

ACCEPTANCE TESTING

610-4.1 ACCEPTANCE SAMPLING AND TESTING. Concrete for each day’s placement will be accepted on the basis of the compressive strength specified in Subsection 610-3.2. The Engineer will sample the concrete in accordance with ATM 501; test the slump in accordance with ATM 503; test air content in accordance with ATM 505; make and cure compressive strength specimens in accordance with ATM 506; and test in accordance with AASHTO T 22.  The Acceptance Testing laboratory will meet the requirements of ASTM C1077.

The Contractor shall provide adequate facilities for the initial curing of cylinders.

610-4.2 DEFECTIVE WORK. Any defective work that cannot be satisfactorily repaired as determined by the Engineer, shall be removed and replaced at the Contractor’s expense. Defective work includes, but is not limited to, uneven dimensions, honeycombing and other voids on the surface or edges of the concrete.

METHOD OF MEASUREMENT

610-5.1 Concrete will be measured by the number of cubic yards based on the dimensions shown on the plans of concrete complete in place and accepted, and according to GCP Section 90. When the pay items shown below are absent from the bid schedule, no measurement for payment will be made.

610-5.2 Steel reinforcement will be measured by the calculated theoretical number of pounds placed, as shown on the Plans, complete in place and accepted. The unit weight used for deformed bars will be the weight of plain square or round bars of equal nominal size. If so indicated on the Plans, the weight to be paid for will include the weight of metal pipes and drains, metal conduits and ducts, or similar materials indicated and included. When the pay items shown below are absent from the bid schedule, no measurement for payment will be made.

BASIS OF PAYMENT

610-6.1 Payment will be made at the contract unit price per cubic yard for structural portland cement concrete and per pound for reinforcing steel. If the following pay items are absent from the bid schedule, no payment will be made.

Payment will be made under:

Item P610.010.0000	Structural Portland Cement Concrete - per cubic yard

Item P610.020.0000	Steel Reinforcement - per pound

References

ATM 304	WAQTC FOP for AASHTO T 27/T 11 Sieve Analysis of Fine and Coarse Aggregates

ATM 501	FOP for WAQTC TM 2 Sampling Freshly Mixed Concrete

ATM 503	WAQTC FOP for AASHTO T 119 Slump of Hydraulic-Cement Concrete

ATM 505	WAQTC FOP for AASHTO T 152 Air Content of Freshly Mixed Concrete by the Pressure Method

ATM 506	WAQTC FOP for AASHTO T 23 Making and Curing Concrete Test Specimens in the Field

AASHTO M 6	Fine Aggregate for Portland Cement Concrete

AASHTO M 43	Sizes of Aggregate for Road and Bridge Construction

AASHTO M 80	Coarse Aggregate for Portland Cement Concrete

AASHTO M 85	Portland Cement

AASHTO M 154	Air-Entraining Admixtures for Concrete

AASHTO M 157	Ready-Mixed Concrete

AASHTO M 182	Burlap Cloth made from Jute or Kenaf and Cotton Mats

AASHTO M 194	Chemical Admixture for Concrete

AASHTO M 213	Preformed Expansion Joint Fillers for Concrete Paving and Structural Construction (Nonextruding and Resilient Bituminous Types)

AASHTO M 295	Coal Fly Ash and Raw or Calcined Natural Pozzolan for Use as a Mineral Admixture in Concrete

AASHTO M 302	Slag Cement for Use in Concrete and Mortars

AASHTO T 22	Compressive Strength of Cylindrical Concrete Specimens

ASTM A184	Welded Deformed Steel Bar Mats for Concrete Reinforcement

ASTM A615	Deformed and Plain Carbon-Steel Bars for Concrete Reinforcement

ASTM A1064	Carbon-Steel Wire and Welded Wire Reinforcement, Plain and Deformed, for Concrete

ASTM C171	Sheet Materials for Curing Concrete

ASTM C309	Liquid Membrane-Forming Compounds for Curing Concrete

ASTM C311	Sampling and Testing Fly Ash or Natural Pozzolans for Use in Portland-Cement Concrete

ASTM C1017	Chemical Admixtures for Use in Producing Flowing Concrete

ASTM C1077	Agencies Testing Concrete and Concrete Aggregates for Use in Construction and Criteria for Testing Agency Evaluation

ASTM C1260	Potential Alkali Reactivity of Aggregates (Mortar-Bar Method)

ASTM C1602	Mixing Water Used in the Production of Hydraulic Cement Concrete

AWS D12.1	Recommended Practices for Welding Reinforcing Steel, Metal Inserts and Connections in Reinforced Concrete Construction

ACI 305R	Hot Weather Concreting

ACI 306R	Cold Weather Concreting

ACI 308R	Guide to External Curing of Concrete

ACI 309R	Guide for Consolidation of Concrete