## ITEM P-621	SAW-CUT GROOVES

DESCRIPTION

621-1.1 This item consists of constructing saw-cut grooves to minimize hydroplaning during wet weather, providing a skid resistant surface in accordance with these specifications and at the locations shown on the plans, or as directed by the Engineer.

CONSTRUCTION METHODS

621-2.1 The Contractor shall submit to the Engineer the grooving sequence and method of placing guide lines to control grooving operation, according to Section 80-03, or as directed by the Engineer.

Transverse grooves saw-cut in the pavement must form a 1/4-inch wide by 1/4-inch deep by 1 1/2 inches center-to-center configuration. The grooves must be continuous for the entire runway length. They must be saw-cut transversely in the runway and high speed taxiway pavement to not less than 10 feet from the runway pavement edge, or as shown in the plans, to allow adequate space for equipment operation.

The saw-cut grooves must meet the following tolerances. The tolerances apply to each day’s production and to each piece of grooving equipment used for production. The Contractor is responsible for all controls and process adjustments necessary to meet these tolerances.

- Alignment tolerance. Plus or minus 1-1/2 inches in alignment for 75 feet.

- Groove tolerance.

  - Depth. The standard depth is 1/4-inch. At least 90 percent of the grooves must be at least 3/16 inch, at least 60 percent of the grooves must be at least 1/4 inch, and not more than 10 percent of the grooves may exceed 5/16-inch.

  - Width. The standard width is 1/4-inch. At least 90 percent of the grooves must be at least 3/16-inch, at least 60 percent of the grooves must be at least 1/4-inch, and not more than 10 percent of the grooves may exceed 5/16-inch.

- Center-to-center spacing. The standard spacing is 1-1/2 inches.

  - Minimum spacing 1-3/8 inches.

  - Maximum spacing 1-1/2 inches.

Saw-cut grooves must not be closer than 3 inches or more than 9 inches from transverse paving joints. Grooves must not be closer than 6 inches and no more than 18 inches from in-pavement light fixtures. Grooves may be continued through longitudinal joints. Where neoprene compression seals have been installed and the compression seals are recessed sufficiently to prevent damage from the grooving operation, grooves may be continued through the longitudinal joints. Where neoprene compression seals have been installed and the compression seals are not recessed sufficiently to prevent damage from the grooving operation, grooves must not be closer than 3 inches or more than 5 inches from the longitudinal joints.  Where lighting cables are installed, discontinue grooving across longitudinal or diagonal saw kerfs.

The Engineer may require the Contractor to submit a written report indicating the percentage of grooves that meet tolerances by measurement zone according to Table 621-1.  If reporting is required, groove tolerance shall be measured at least three times per zone per day.  The Engineer may require a report indicating how many times production was adjusted.  It is expected that the Contractor will routinely spot check for compliance each time the equipment aligns for a grooving pass.  The Engineer may determine a written report is not required.

Blade wear and surface variability may require more testing than the minimum of three per day per zone during each day’s production.

621-2.2 ENVIRONMENTAL REQUIREMENTS. Grooving operations will not be permitted when freezing conditions prevent the immediate removal of debris and/or drainage of water from the grooved area.

621-2.3 CONTROL STRIP.  Groove a control strip in an area of pavement outside of the trafficked area, or as approved by the Engineer.  The area shall be as long as the width of the runway or taxiway, or at least 25 feet in length, by two passes of the grooving machine, or as required by the Engineer.  Demonstrate the setup and alignment process, the grooving operation, and the waste slurry disposal.

621-2.4 EXISTING PAVEMENTS. Bumps, depressed areas, bad or faulted joints, and badly cracked and/or spalled areas in the pavement shall not be grooved until such areas are adequately repaired or replaced.

621-2.5 NEW PAVEMENTS. New asphalt and Portland cement concrete pavements shall be allowed to cure for a minimum of 30 days before grooving, to allow the material to become stable enough to prevent closing of the grooves under normal use.  All grade corrections must be completed prior to grooving.  Spalling along or tearing or raveling of the groove edges shall not be allowed.

The Engineer may allow grooving after a curing period of less than 30 days if it can be demonstrated that grooves are stable with no spalling along or tearing or raveling of the groove edges.

621-2.6 GROOVING MACHINE.  Provide a grooving machine that is power driven, self-propelled, specifically designed and manufactured for pavement grooving, and has a self-contained and integrated continuous slurry vacuum system as the primary method for removing waste slurry.  The grooving machine shall be equipped with diamond-saw cutting blade groove cutting head capable of making at least 18 inches in width of multiple parallel grooves in one pass of the machine. Thickness of the cutting blades shall be capable of making the required width and depth of grooves in one pass of the machine. The cutting head shall not contain a mixture of new and worn blades or blades of unequal wear or diameter. Match the blade type and configuration with the hardness of the existing airfield pavement. The wheels on the grooving machine shall be of a design that will not scar or spall the pavement. The machine must be equipped with devices to control depth of groove and alignment.

621-2.7 WATER SUPPLY. Water for the grooving operation shall be provided by the contractor.

621-2.8 CLEAN-UP. During and after installation of saw-cut grooves, the Contractor must remove from the pavement all debris, waste, and by-products generated by the operations to the satisfaction of the Engineer. Cleanup of waste material must be continuous during the grooving operation. Flush debris produced by the machine to the edge of the grooved area or pick it up as it forms. The dust coating remaining shall be picked up or flushed to the edge of the area if the resultant accumulation is not detrimental to the vegetation or storm drainage system. Accomplish all flushing operations in a manner to prevent erosion on the shoulders.  Waste material must be disposed of in an approved manner. Waste material must not be allowed to enter the airport storm or sanitary sewer system. The Contractor must dispose of these wastes in strict compliance with all applicable state, local, and Federal environmental statutes and regulations.

621-2.9 REPAIR OF DAMAGED PAVEMENT. Grooving must be stopped and damaged pavement repaired at the Contractor's expense when directed by the Engineer.

ACCEPTANCE

621-3.1 ACCEPTANCE TESTING. Grooves will be accepted based on results of zone testing. All acceptance testing necessary to determine conformance with the groove tolerances specified will be performed by the Engineer.

Instruments for measuring groove width and depth must have a range of at least 0.5-inch and a resolution of at least 0.005-inch. Gage blocks or gages machined to standard grooves width, depth, and spacing may be used.

Instruments for measuring center-to-center spacing must have a range of at least 3 inches and a resolution of at least 0.02-inch.

The Engineer will measure grooves in five zones across the pavement width. Measurements will be made at least three times during each day’s production. Measurements in all zones will be made for each cutting head on each piece of grooving equipment used for each day’s production.

The five zones are as shown in Table 621-1:

TABLE 621-1. DEFINITION OF MEASUREMENT ZONES

| ZONE Number | ZONE Position |
| --- | --- |
| Zone 1 | Centerline to 5 feet left or right of the centerline. |
| Zone 2 | 5 feet 25 feet left of the centerline. |
| Zone 3 | 5 feet to 25 feet right of the centerline. |
| Zone 4 | 25 feet to edge of grooving left of the centerline. |
| Zone 5 | 25 feet to edge of grooving right of the centerline. |

At a random location within each zone, five consecutive grooves sawed by each cutting head on each piece of grooving equipment will be measured for width, depth, and spacing. The five consecutive measurements must be located about the middle blade of each cutting head plus or minus 4 inches. Measurements will be made along a line perpendicular to the grooves.

- Width or depth measurements less than 0.170-inch will be considered less than 3/16-inch.

- Width or depth measurements more than 0.330-inch will be considered more than 5/16-inch.

- Width or depth measurements more than 0.235-inch will be considered more than 1/4inch.

Production must be adjusted when more than one groove on a cutting head fails to meet the standard depth, width, or spacing in more than one zone.

METHOD OF MEASUREMENT

621-4.1 Pavement saw-cut grooves will be measured either by neat line dimensions as shown in the Plans or as a single item of work. No deductions will be made for areas skipped to avoid joints or in-pavement fixtures.

BASIS OF PAYMENT

621-5.1 Payment will be made at the contract unit price or the lump sum price for pavement saw-cut grooves accepted by the Engineer.

Payment will be made under:

Item P621.010.0000	Saw-Cut Grooves - per square yard

Item P621.020.0000	Saw-Cut Grooves - per lump sum