## ITEM P-661 STANDARD SIGNS

DESCRIPTION

661-1.1 Furnish and install standard signs. The location and type of installation will be as shown on the plans or as designated.

MATERIALS

661-2.1 Use materials that conform to the following:

- Sheet Aluminum. Use alloy 6061-T6, 5052-H36, 5052-H38, or recycled aluminum meeting alloy 3105, as specified in ASTM B 209. Meet the thickness of aluminum sheet designated on the plans. Verify alloy and temper designations by mill certification.

Treat the aluminum base metal sheets with coating for aluminum to meet ASTM B921, Class 2. Handle the cleaned and coated base metal only by a mechanical device or by operators wearing clean cotton or rubber gloves. After cleaning and coating operations, protect the panels at all times from contact or exposure to greases, oils, dust or other contaminants.

Make each sign panel a continuous sheet for all lengths 72 inches or less in the horizontal direction. Use no more than one vertical splice for signs up to 144 inches in length and 48 inches or less in height.

Meet the panel dimensions specified with a tolerance of 1/16-inch. Furnish metal panels that are cut to size and shape and free of buckles, warp, dents, cockles, burrs and any other defects resulting from fabrication. Complete all possible fabrication, including shearing, cutting and punching of holes prior to the base metal preparation.

- Retroreflective Sheeting. Meet ASTM D4956, for the type specified.

- Sign Posts. Use the type and size of posts designated on the plans.

  - Perforated Steel Posts.

Fabricate posts from 0.105-inch thick cold-rolled carbon steel sheets, commercial quality, to meet ASTM A 653 and ASTM A 924. Zinc coat, both sides, to meet coating designation G90. Form posts into a steel tube, roll to size, and weld in the corner.

Perforate all members for their entire length with 7/16-inch diameter holes on 1-inch centers.

Furnish members that are straight and with a smooth, uniform finish, with no splices.

Ensure that all perforations and cut off ends are free from burrs.

Ensure that consecutive sizes will telescope freely with a minimum of play.

- Sign Fabrication. Use Type IV retroreflective sheeting (for lettering, symbols, borders, and background) on sheet aluminum panels.

- Sign Posts and Bases. Use sign posts and bases of the types specified. The structural aspects of design and materials for sign supports must comply with the AASHTO Standard Specifications for Structural Supports for Highway Signs, Luminaires, and Traffic Signals. Do not splice sign posts.

Use commercial grade concrete for sign foundations with a minimum 28-day compressive strength of 2,500 psi or an approved, pre-mixed, sacked concrete.

CONSTRUCTION REQUIREMENTS

661-3.1 Attach sign panels to posts using the types and sizes of fastening hardware shown on the plans.

All materials and finished signs are subject to inspection and acceptance in place.

a.	Surfaces exposed to weathering must be free of defects in the coating that impair serviceability or detract from general appearance or color match.

- Finished signs must be clean and have no chatter marks, burrs, sharp edges, loose rivets, delaminated retroreflective sheeting, or aluminum marks. Do not make repairs to the face sheet.

Install breakaway assemblies according to the manufacturer’s written instructions.

Remove and replace all foundations requiring more than three shims to plumb a post without extra compensation.

Construct the top of any foundation located on a slope so that the finished slope passes through the top center of the foundation. Grade the area 24 inches up and down slope of the foundation edge so that no portion of the foundation projects above the surrounding slope and water will drain away from the foundation.

Attach a label to the back of all standard signs in the lower right corner. Make the label at least 15 square inches and show the year the sign was purchased from the manufacturer. Show the last two digits of the year in clear and bold numbers. Make the label from Type I or brighter reflective sheeting. Use background and legend colors meeting Table 661-1.

Table 661-1

DECAL COLORS

| YEAR | BACKGROUND COLOR | LEGEND COLOR |
| --- | --- | --- |
| XXX1 | Yellow | Black |
| XXX2 | Red | White |
| XXX3 | Blue | White |
| XXX4 | Green | White |
| XXX5 | Brown | White |
| XXX6 | Orange | Black |
| XXX7 | Black | White |
| XXX8 | White | Black |
| XXX9 | Purple | White |
| XXX0 | Strong Yellow-Green | Black |

Central values and tolerance limits for each color, as referenced in the MUTCD, are available from the Federal Highway Administration, (HHS-30), 400 7th St. SW, Washington, D.C. 20590

661-3.2 Sign Placement And Installation. Sign locations are approximate and subject to field adjustment by the Engineer.

Do not allow the top of the embedded steel tube to extend more than 2 inches above the surrounding ground and concrete foundation.

On all signs, install 2-inch diameter wind washers, colored to match the sign face, between the fastener head and the sign. Use rust-resistant washers fabricated from a material equal in strength to the sign blank.

METHOD OF MEASUREMENT

661-4.1 By the total area of legend-bearing sign panel erected in place. No deductions in quantity for corner rounding will be made. Nominal dimensions for sign sizes indicated on the plans will be used to calculate sign pay quantities. Octagons and round signs will be measured as rectangles.

BASIS OF PAYMENT

661-5.1 Payment will be made at the contract price per unit of measurement. Sign posts, bases, mounting hardware, and concrete used for sign bases are subsidiary.

Payment will be made under:

Item P661.010.0000	Standard Sign – per square foot