## ITEM P-671	RUNWAY AND TAXIWAY CLOSURE MARKERS

DESCRIPTION

671-1.1 Furnish, install, and maintain runway and/or taxiway closure markers at the locations shown on the Plans or as directed by the Engineer. Where a new runway is built to replace an existing runway, install runway closure markers on the old runway immediately after the new runway has been opened for operations. Place markers as shown on the Plans or as directed by the Engineer. Relocate markers as required. Materials supplied under this item may be used as temporary closure markers as required in GCP Subsection 80-04.

MATERIALS

671-2.1 Use materials that conform to the following.

- Vinyl Mesh Panel.

  - Panel Material. High tenacity vinyl coated polyester mesh fabric, 9 ounces per square yard (oz/yd2), 70% closed mesh allowing water to flow through. Use 3.0 oz/yd2 woven polyester fabric, coated after weaving with 6.0 oz/yd2 coating of poly vinyl chloride, color traffic yellow. Minimum tensile strength 230 by 200 pounds (lbs) grab method and 200 by 140 lbs strip method. Meet ASTM D 471 for water absorption, 7 days @160°F, 5.0% maximum weight gain and ASTM D 750 for weathering, 2,500 hours, no appreciable change in color, no cracking, minimum crazing.

  - Seams, Perimeter Hem, and Thread. Double flat felled seams, double stitched, and 3-ply perimeter hem sewn with UV resistant #92 bonded polyester thread.

  - Grommets. No. 2 brass rolled-rim spur grommets installed through hem at 30-inch intervals along marker perimeter.

  - Anchors. 3/8-inch diameter deformed reinforcing steel at least 18 inches long, including a hook formed as a 4-inch segment bent perpendicular to the anchor stem.

- Snow Fence Panel.

  - Panel Material. Wire-supported wood lathe snow fence, pre-treated with a suitable wood stain.

  - Paint Type: (select one)

    - AASHTO M248, Type F (Alkyd resin)

    - FSS TT-P-19D(1) Paint Latex (Acrylic emulsion, Exterior).

  - Paint Color: Traffic Yellow, #33538

  - Anchors: 3/8-inch diameter deformed reinforcing steel at least 18 inches long, including a hook formed as a 4-inch segment bent perpendicular to the anchor stem.

- Temporary Illuminated Panel.

  - Federal Aviation Administration (FAA) Advisory Circular (AC) 150/5345-53, Airport Lighting Equipment Certification Program (ALECP). The AC 150/5345-53, the latest certified equipment list, and the address list of certified airport lighting equipment manufacturers are available on the FAA webpage at: https://www.faa.gov/airports/engineering/airport_lighting/.

CONSTRUCTION REQUIREMENTS

671-3.1 Meet the following requirements.

- Vinyl Mesh Panel. Secure by driving anchors into the embankment through all grommets.

- Snow Fence Panel. Apply to the upper side of the panels, two coats of paint that result in a dense and consistent color. Construct panels double layered, with upper layer wood lathe oriented to lower lathe at right angles to provide a solid yellow appearance.

Combine standard manufactured widths to provide plan dimensions, if necessary.

Secure panels by driving anchors into the embankment at 30-inch intervals around the perimeter of each panel. If more than one standard manufactured width is combined to obtain plan dimensions, provide anchors on each strip.

- Temporary Illuminate Panel. Locate the marker where shown on the plans or as directed by the Engineer. The contractor shall maintain an uninterrupted operation of the closure marker. Maintenance records shall be kept by the Contractor for all portable lighted markers and will be turned in to the Engineer when construction is complete.

METHOD OF MEASUREMENT

671-4.1 By the number of markers of the specified type, installed and accepted as completed units in place. No additional measurement will be made for removing and relocating markers for various stages of work.

BASIS OF PAYMENT

671-5.1 Payment will be made at the contract unit price for each furnished and accepted item of the marker type specified.

Payment will be made under:

Item P671.___.____      Runway Closure Marker, ____ – per each

Item P671.___.____	Taxiway Closure Marker, ____ – per each

TESTING REQUIREMENTS

ASTM D 471	Rubber Property – Effect of Liquids

ASTM D 750	Rubber Deterioration in Carbon-Arc Weathering Apparatus