## ITEM P-680	GEOTEXTILE FOR SILT FENCE

680-1. 1 DESCRIPTION. Furnish, install, maintain, and remove temporary silt fence as shown on the Plans or as directed.

MATERIALS

680-2.1 SILT FENCE.  Meet AASHTO M 288 for Temporary Silt Fence.

- Prefabricated Silt Fence	Meet the Plans and Section P-680 requirements.

- Attachment Devices	Staples; wire; self-locking nylon, plastic, wire ties; or other approved means to attach fabric to posts.

- Support Mesh between Posts	14-gage welded wire fencing, metal chain-link fabric, or geosynthetic mesh with equivalent strength.  Use maximum mesh spacing of 6 inches.  Use height shown on the Plans, or specified in the Bid Schedule.

- Posts	Wood 1.5-inch x 1.5-inch x 36-inch minimum, steel, or approved synthetic material.

CONSTRUCTION REQUIREMENTS

680-3.1 INSTALLATION. Install silt fence according to Plans.  Use Trenchless Detail when installing silt fence over permanently frozen ground.  Drill holes for support posts, if required.

When joining to another roll, place both end posts together and wrap them with silt fence by turning them one full rotation. Drive the wrapped posts.

680-3.2 MAINTENANCE. Maintain the integrity of the fence to contain sediment in runoff until final stabilization.

680-3.3 REMOVAL. After disturbed area has been accepted as permanently stabilized or when sediment protection is no longer needed, remove silt fence.

680-4.1 METHOD OF MEASUREMENT. See Section 90. Measure silt fence by the length of fence installed.  No allowance will be made for overlap, whether at joints or patches.

680-5.1 BASIS OF PAYMENT. The contract price includes installation, maintenance, removal and disposal of the silt fence.

Payment will be made under:

Item P680.010.0000	Silt Fence – per linear foot