## ITEM P-684	FLOATING SILT CURTAIN

DESCRIPTION

684-1.1 Furnish, place, maintain, and remove temporary floating silt curtain as shown on the Plans for control of sediment and debris.

MATERIALS

684-2.1 GENERAL. Provide a silt curtain of commercial manufacture, with demonstrated ability to trap and hold sediment and debris.

684-2.2 SUBMITTALS AND APPROVAL. Submit for approval of the silt curtain that is proposed for use in the work. Obtain approval prior to shipment to the project site. Provide submittals that include certificates of compliance, manufacturer’s printed instructions and/or shop drawings and proposed installation/removal procedures.

684-2.3 CURTAIN FABRIC. For curtains used in standing water, provide pervious geotextile meeting AASHTO M 288 for Temporary Silt Fence or impervious coated fabric such as nylon reinforced polyvinyl chloride, treated polypropylene/polyester fabric or approved equal adhering to the following:

| Grab tensile strength (ASTM D4632 or equivalent) | 200 lb |
| --- | --- |
| Maximum apparent opening size (ASTM D4751 or equivalent) | 0.008 inch |
| UV3 Resistance | Required |
| Panel Lengths | 100 feet or less (for depths less than 13 feet) |

684-2.4 FLOTATION. Provide Flotation consisting of rigid, closed cell expanded polystyrene, ethafoam or polyethylene floats attached to the top of the silt curtain along its entire length. Provide flotation material with protection from mechanical damage and deterioration that would cause pollution. Employ flotation that provides the curtain with a minimum of free board without gaps. Ensure that the buoyancy ratio (weight of displaced fluid to barrier weight) is greater than 3 to 1.

Provide high visibility color fabric cover for the flotation devices with a 1-inch minimum width reflective band attached on the side of the flotation covering along the entire length of the boom. Ensure that the flotation is secured to the boom to prevent shifting or slipping. Provide manufacturer installed grommets or equivalents to reinforce stress points and provide attachment points.

684-2.5 LINES AND ATTACHMENT POINTS. Provide a curtain that incorporates anchor lines, top load lines and bottom load lines, as required, that are minimum 1/2-inch diameter nylon rope. Provide a curtain with anchor lines, additional ballast, and floats that are attached to the silt curtain at reinforced attachment points provided by the manufacturer.

684-2.6 ANCHOR/BALLAST. Provide anchor and ballast chain of minimum 1/2-inch diameter galvanized steel with ballast chain sewn into a hem at the bottom of the curtain and secured to the material of the hem to prevent shifting or accidental removal.

CONSTRUCTION REQUIREMENTS

684-3.1 GENERAL. Provide a curtain high enough to extend to the bottom of the water channel plus 10 %. Weight the base of the curtain with ballast so that it will remain in continuous contact with the bottom to prevent sediment and silt migration.

Maintain the silt curtain in a basically vertical position. Allow a minimum of 6 inches free board at the top of the curtain for curtain depths less than 6.5 feet and 12 inches free board for curtain depths more than 6.5 feet at all times along its continuous length.

684-3.2 JOINING PANELS/SECTIONS. For ease of handling and transportation, individual panels/sections may be connected or sewn together in the field. Do not use heat welding methods to join panels. Join the panels in a manner that will prevent silt, sediment, debris or turbidity to migrate from the work area. If joints are sewn together, use heavy duty #350 polyester twine thread to make double row 1/4-inch maximum stitches that will not unravel if broken.

684-3.3 CONDITIONS AND TIMING FOR INSTALLATION. Install silt curtain instead of silt fence when fence free board is anticipated to be less than 1-foot or as directed by the Engineer. Install as soon as open water appears in the spring and before the embankment begins to thaw.

684-3.4 ANCHORS. Provide anchors in the size and number required to maintain the curtain in position for proper and continuous operation once deployed. Mark the vertical position of the anchors with crown buoys to warn of their hazard and facilitate easy recovery.

Attach anchor chains between the anchor line and anchor to prevent line fouling, to lower the angle of load pulling on the anchor, and to act as a shock absorber.

Employ anchor line buoys to help prevent line entanglement and stress on the boom.

Equip each anchor with a minimum of 10 feet of anchor chain.

684-3.5 MAINTENANCE. After installation, maintain the floating silt curtain in proper working order until the embankment has 70 percent vegetative cover. Maintain curtain used to control other areas of the work until sediment in suspension has settled and floating debris has been removed. Removal must be approved by the Engineer. Conduct the removal during periods of calm weather. Remove the curtain carefully to minimize the release of trapped sediment and debris. Do not drag the curtain while in contact with the water channel bottom.

Maintain the integrity of the curtain as long as it is necessary to contain sediment. Inspect daily and correct deficiencies immediately. Remove and dispose of the curtain when adequate vegetative growth insures no further erosion of the slopes.

METHOD OF MEASUREMENT

684-4.1 See Section 90. At the water line along the face of the flotation at the contract price per foot.

BASIS OF PAYMENT

684-5.1 Payment will be made as follows: 60 percent for installation. 25 percent for maintenance and repairs, prorated over the anticipated active construction period with a portion included as part of each interim payment. If the anticipated construction period changes, the remainder for maintenance will be prorated over the new period. 15 percent for removing it from the site.

Payment will be made under:

Item P684.010.0000	Floating Silt Curtain – per linear foot