## ITEM P-686	FIBER ROLL

DESCRIPTION

686-1.1 Furnish, place, maintain, and remove fiber rolls as shown on the Plans or as directed.

MATERIALS

686-2.1 FIBER ROLL.  Fiber Rolls shall be constructed with a pre-manufactured blanket consisting of either wood excelsior, rice or wheat straw, or coconut fibers or a combination of these materials.  The blanket shall be between 6 feet and 8 feet in width and between 65 feet and 95 feet in length.  Wood excelsior shall be individual fibers, of which 80 percent shall be 6 inches or longer in length. The blanket shall have a photodegradable plastic netting or biodegradable jute, sisal, or coir fiber netting on at least one side.  The blanket shall be rolled along the width and secured with jute twine spaced 6 feet apart along the full length of the roll and placed 6 inches from the ends of each roll.  The finished roll shall be between 8 inches and 10 inches in diameter, a minimum of 20 feet in length, and shall weigh a minimum of 0.5 pound per linear foot.  More than one blanket may be required to achieve the finished roll diameter.  When more than one blanket is required, blankets shall be jointed longitudinally with an overlap of 6 inches along the length of the blanket.

686-2.2 STAKES. Wood stakes shall be a minimum of 1-inch by 1-inch by 24 inches long in size.  Wood stakes shall be untreated fir, redwood, cedar, or pine and cut from sound timber.  They shall be straight and free of loose or unsound knots and other defects which would render them unfit for the purpose intended. Metal stakes shall not be used.

CONSTRUCTION REQUIREMENTS

686-3.1 Install fiber rolls before excavation or embankment construction begins.

686-3.2 INSTALLATION. Fiber rolls shall be installed as follows:

- Furrows shall be constructed to a depth between 2 inches and 4 inches, and to a sufficient width to hold the fiber roll.  Stakes shall be installed 24 inches apart along the length of the fiber rolls and stopped at 12 inches from each end of the rolls.  Stakes shall be driven to a maximum of 2 inches above, or flush with the top of the roll.

- Fiber rolls shall be placed 10 feet apart along the slope for slope inclination (horizontal:vertical) of 2:1 and steeper, 15 feet apart along the slope for slope inclination of 2:1 and 4:1, 20 feet apart along the slope for slope inclination between 4:1 and 10:1, and a maximum of 50 feet apart along the slope for slope inclination of 10:1 and flatter.

- The bedding area for the fiber roll shall be cleared of obstructions including rocks, clods, and debris greater than 1-inch in diameter before installation.

- Fiber rolls shall be installed approximately parallel to the slope contour.

- Fiber rolls shall be installed before the application of other temporary erosion control or soil stabilization materials in the same area.

686-3.3 MAINTENANCE AND REMOVAL. Fiber rolls shall be maintained to disperse concentrated water runoff and to reduce runoff velocities.  Split, torn, or unraveled rolls shall be repaired or replaced.  Broken or split stakes shall be replaced.  Sagging or slumping fiber rolls shall be repaired with additional stakes or replaced.  Locations where rills or other evidence of concentrated runoff have occurred beneath the rolls shall be corrected.  Fiber rolls shall be repaired or replaced within 24 hours of identifying the deficiency.

When no longer required, as determined by the Engineer, fiber rolls shall be removed and disposed.  The fiber rolls may be abandoned in place when approved in writing by the Engineer. If approved, the stakes shall be removed or pounded into the ground.

METHOD OF MEASUREMENT

686-4.1 Fiber rolls shall be measured by the linear foot measured along the centerline of the installed roll.  Where fiber rolls are joined and overlapped, the overlap will be measured as a single installed roll.

BASIS OF PAYMENT

686-5.1 Payment will be made at the contract unit price per linear foot for fiber roll.  Payment includes full compensation for furnishing all labor, materials, tolls, equipment, and incidentals, and for doing all the work involved in stalling fiber rolls, complete in place, including furrow excavation and backfill, maintenance, and removal.  Damage to fiber rolls resulting from the Contractor’s vehicles, equipment, or operations shall be repaired at the Contractor’s expense. If the following pay item is absent from the bid schedule, no payment will be made, and all work, materials, and equipment required to complete the work will be subsidiary to pay item P641.030.0000 Temporary Erosion, Sediment and Pollution Control.

Payment will be made under:

Item P686.010.0000	Fiber Roll – per linear foot