## ITEM T-905	TOPSOIL

DESCRIPTION

905-1.1 This item shall consist of preparing the ground surface for topsoil application, removing topsoil from designated stockpiles or areas to be stripped on the site or from approved sources off the site, and placing and spreading the topsoil on prepared areas in accordance with this specification at the locations shown on the plans or as directed by the Engineer.

MATERIALS

905-2.1 TOPSOIL. Provide a natural friable surface soil without admixtures of undesirable subsoil, refuse, or foreign materials and reasonably free from roots, clods, hard clay, noxious weeds, tall grass, brush sticks, stubble or other litter, and which is free draining and non-toxic.

The gradation shall conform to selected Class in Table 1 when tested according to ATM 304 If no class is indicated, meet the grading requirements in Table 1 for Class A topsoil.

TABLE 1

TOPSOIL GRADING

| Sieve Designation | Percent Passing By Weight |
| --- | --- |
|  | CLASS A | CLASS B |
| 3 in | - | 100 |
| 1/2 in. | 100 | - |
| No. 4 | 95-100 | 75-100 |
| No. 16 | 64-90 | 50-95 |
| No. 200 | 30-60 | 20-80 |
| Organic Matter | 10-40 | 5 min. |

Percent of organic matter will be determined by loss-on-ignition of oven dried samples using ATM 203.

When necessary, amend natural topsoil to meet the above specifications, using approved materials and methods.

CONSTRUCTION METHODS

905-3.1 PREPARING THE GROUND SURFACE. Where grades in the areas to be topsoiled have not been established, smooth-grade the areas to the grades shown on the Plans. Maintain the prescribed grades in an even and properly compacted condition to prevent the formation of low places or pockets where water will stand.

Clear the surface of the area to be topsoiled of all stones larger than 2 inches in any diameter and all litter or other material which may be detrimental to proper bonding, the rise of capillary moisture, or the proper growth of the desired planting.

Immediately prior to dumping and spreading the topsoil, loosen the surface, by approved means, to a minimum depth of 2 inches to facilitate bonding of the topsoil to the covered subgrade soil.

905-3.2 OBTAINING TOPSOIL. Prior to the stripping of topsoil from designated areas, remove any vegetation, stumps and large roots, rubbish or stones found on such areas, which may interfere with subsequent operations, using approved methods.

When suitable topsoil is available on the site, remove this material from the designated areas to the depth directed. Spread the topsoil on areas already tilled and smooth-graded, or stockpile in approved areas. Grade the stockpile sites and adjacent areas which have been disturbed if required and put into a condition acceptable for seeding.

When suitable topsoil is secured off the airport site, locate and obtain the supply, subject to approval. Notify the Engineer sufficiently in advance of operations in order that necessary measurements and tests can be made. Remove the topsoil from approved areas and to the depth as directed. Haul the topsoil to the site of the work and stockpile or spread as required.

905-3.3 PLACING TOPSOIL. Spread the topsoil evenly on the prepared areas to a uniform depth of 4 inches after compaction. Do not spread when the ground or topsoil is frozen or excessively wet.

After spreading, break up any large stiff clods and hard lumps with a pulverizer or other effective means. Rake up and dispose of all stones or rocks (2 inches or more in diameter), roots, litter, or any foreign matter. After spreading, compact the topsoil with a cultipacker or by other approved means. The compacted topsoil surface shall conform to the required lines, grades, and cross sections. Promptly remove any topsoil or other dirt falling upon pavements or other surface courses.

Track topsoil with a dozer to make track marks running perpendicular to the direction of drainage.

METHOD OF MEASUREMENT

905-4.1 By the square yard, according to GCP Subsection 90-02, acceptably placed.

BASIS OF PAYMENT

905-5.1 Payment will be made at the contract unit price per square yard.

Stockpiling and rehandling of topsoil are subsidiary.

Payment will be made under:

Item T905.010.____	Topsoiling, Class ____ – per square yard

TESTING REQUIREMENTS

ATM 304	WAQTC FOP for AASHTO T 27/T 11 Sieve Analysis of Fine and Coarse Aggregates